NFA36205 A 48 CP,AP,FP steel plate/sheet for Boilers and Pressure Vessels
Key words :
A 48 CP,AP,FP steel plate/sheet, NFA36205 A 48 CP,AP,FP steel plate/sheet, NFA36205 A 48 CP,AP,FP steel plate/sheet for Boilers and Pressure Vessel steel, A 48 CP,AP,FP steel plate/sheet for Boilers and Pressure Vessel, NFA36205 steel plate for Boilers and Pressure Vessel using, A 48 CP,AP,FP steel supplier/Chinese supplier, A 48 CP,AP,FP steel price...

Equivalent grade :
A 48 CP,AP,FP steel plate/sheet is in NFA36205 standard. The equal material of A 48 CP,AP,FP steel is: DIN17165 19 Mn 8 , EN 10028-3 P 355 N, EU 113 Fe E 355

| A 48 CP,AP,FP NFA36205 | Comparison of steel grades |
| --- | --- |
|  | EN 10028-3 | P 355 N |
|  | EU 113 | Fe E 355 |
|  | DIN17165 | 19 Mn 8 |
|  | NFA36205 | A 52 CP,AP,FP |

NFA36205 A 48 CP,AP,FP steel Chemical Composition % : 
Main chemical composition in NFA36205 A 48 CP,AP,FP steel: Carbon Max 0.09, Manganese Max 1.05, Silicon max 0.50, Ni Max 0.90,  More detailed information, please refer to the flowing table:

NFA36205 A 48 CP,AP,FP steel  steel Chemical Composition %

| Grades | C max | Si max | Mn max | Ni max |
| --- | --- | --- | --- | --- |
| A 48 CP,AP,FP | 0.09 | 0.5 | 1.05 | 0.9 |

NFA36205 A 48 CP,AP,FP steel Mechanical Properties  
A 48 CP,AP,FP this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is 470 MPa, A 48 CP,AP,FP tensile strength is from 560MPa. (different min strength point at the different thickness.) More detailed information about NFA36205 A 48 CP,AP,FP steel Mechanical Properties , please refer to the following table:

| Thickness | Yield Strength ReH[N/mm2] transv.min | Tensile Strength Rm[N/mm2]transv | Fracture Elongation [%]transv. min. | Notch Impact Energy1) Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t >16mm | 470 | 560 | 24 | - |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.