Key words: A 572 Gr. 50 steel plate/sheet, ASTM - SAE A 572 Gr. 50 steel plate/sheet, A 572 Gr. 50 steel plate/sheet supplier/Chinese supplier, A 572 Gr. 50 steel plate/sheet mechanical property, A 572 Gr. 50steel plate/sheet price.

ASTM A 572 Gr. 50 steel equivalent grade:
A 572 Gr. 50 steel plate/sheet is in ASTM standard, the grade number is 1.0545. The equivalent material of A 572 Gr. 50 steel are UNI7382 FeE355KG, EN 10028-3 P355N, UNE36081 AE355KG, DIN 1614/2 A572Gr50.

| A572Gr50 ASTM MATERIAL# 1.0562 | Comparison of steel grades |
| --- | --- |
|  | UNI7382 | FeE355KG |
|  | EN 10028-3 | P355N |
|  | UNE36081 | AE355KG |
|  | DIN 1614/2 | A572Gr50 |

ASTM A 572 Gr. 50 steel chemical composition %:
Main chemical composition in ASTM - SAE A 572 Gr. 42 steel is carton max 0.09, silicon max 0.50, manganese max 1.05, nickel max 0.9. More detailed information about A 572 Gr. 50 steel, please refer to the down table:

| Grades | C | Si | Mn | Ni |
| --- | --- | --- | --- | --- |
|  | max | max | max | max |
| A 572 Gr50 | 0.09 | 0.5 | 1.05 | 0.9 |

ASTM A 572 Gr. 50 steel mechanical property:
A572Gr 50 steel plate, ASTM- SAE A572Gr50 steel plate, under ASTM standard, we can regard A572Gr50 steel plate as Fine-grain structural steels, normalised rolled steel.

| Thickness | Yield Strength ReH[N/mm2] transv.min | Tensile Strength Rm[N/mm2]transv | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t >16mm | 470 | 560 | 24 | - |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of ASTM - SAE A 572 Gr. 50 steel are available, so if need, welcome to contact ICE steel sales team.