ASTM A 572gr. 60,65 steel plate/sheet for High Yield Steel

Key words: A 572gr. 60,65 steel plate/sheet, ASTM A 572gr. 60,65 steel plate/sheet, A 572gr. 60,65 steel plate/sheet supplier/Chinese supplier, A 572gr. 60,65 steel plate/sheet price, A 572gr. 60,65 steel plate/sheet mechanical property.

ASTM A 572gr. 60,65 steel equivalent grade:
A 572gr. 60,65 steel plate/sheet is in ASTM standard, the equivalent grade are DIN 17102 STE 380, NFA 36201 E 375R, MNC 810E SS21,42,01, CSA G40-21 400 W, WT, JIS 3101 SS 540.

| A 572gr. 60,65 ASTM | Comparision of steel grades |
| --- | --- |
|  | DIN 17102 | STE 380 |
|  | NFA 36201 | E 375R |
|  | MNC 810E | SS21,42,01 |
|  | CSA G40-21 | 400 W, WT |
|  | JIS 3101 | SS 540 |

ASTM A 572gr. 60,65 steel chemical composition %:
Main chemical composition in ASTM A 572gr. 60,65 steel is carton max 0.26, silicon max 0.40, manganese max 1.35, phosphorus max 0.04, Sulphur max 0.05. More detailed information about A 572gr. 60,65 steel, please refer to the down table:

| Symbol | Chemical composition |
| --- | --- |
|  | C max | Si max | Mn max | P max | S max |
| Grade60 | 0.26 | 0.40 | 1.35 | 0.04 | 0.05 |
| Grade65 | 0.26 | 0.40 | 1.35 | 0.04 | 0.05 |

ASTM A 572gr. 60,65 steel mechanical property:
A 572Gr60/65 steel plate is one mainly of High Yield steel ASTM A572Gr60,65 is high strength low alloy steel plate sheet which is widely used in plants building, general mansions and all kinds of construction machinery, such as mines and various types of drilling rig used in construction, power shovel, electric wheel dump trucks, mining vehicles, excavators, loaders, bulldozers , various types of cranes, hydraulic support, coal mining machinery and equipments and other structures.

| Symbol | Yield point min MPa | Tensile strength MPa | Elongation in 2 in.(50mm)% |
| --- | --- | --- | --- |
| Grade A | 165 | 310-450 | 30 min |
| Grade B | 185 | 345-450 | 28 min |
| Grade C | 205 | 380-515 | 25 min |
| Grade D | 230 | 415-550 | 23 min |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of ASTM A 572gr. 60,65 steel are available, so if need, welcome to contact ICE steel sales team.