ASTM A 622GR.A,B,C boilers and Pressure Vessels steels
Key words :
ASTM A 622GR.A,B,C steel plate/sheet, ASTM A 622GR.A,B,C steel plate/sheet, under ASTM standard, we can regard A 622GR.A,B,C steel plate/sheet for boilers and Pressure Vessels steels. ASTMA 622GR.A,B,C steel plate/sheet is for boilers and Pressure Vessels steels, it is a normalized steel plate and sheet which is mainly used for building pressure vessels and boilers and pipes for hot liquid.
If you are looking for Chinese A 622GR.A,B,C steel supplier, if you want to know A 622GR.A,B,C steel price, please be free to contact us

ASTM A622GR.A,B,C  steel Chemical Composition % : 
Main chemical composition in ASTM A622GR.A,B,C  steel: Carbon max 0.18, Manganese from 0.90 to 1.70, Sulphur max 0.03, Phosphorus max 0.03, Silicon max 0.50, More detailed information, please refer to the flowing table:

| Element | Max % | Element | max % |
| --- | --- | --- | --- |
| C | 0.18 | Cu | 0.30 |
| Si | 0.50 | Mo | 0.08 |
| Mn | 0.90-1.70 | N | 0.02 |
| P | 0.03 | Nb | 0.05 |
| S | 0.03 | Ni | 0.50 |
| AL | - | Ti | 0.03 |
| Cr | 0.30 | V | 0.10 |
| Nb+Ti+V | 0.12 |  |  |

ASTM A622GR.A,B,C steel Mechanical Properties 
A622GR.A,B,C this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 295- 355 MPa (there is different min strength point at the different thickness.) A622GR.A,B,C tensile strength is from 450MPa to 630MPa. (different min strength point at the different thickness.) More detailed information about ASTM A622GR.A,B,C steel Mechanical Properties , please refer to the following table:

| Grade | Material | Thickness | Yield Strength | Tensile Strength | Elongation |
| --- | --- | --- | --- | --- | --- |
|  |  | (mm) | MPa (min) | MPa | % (min) |
| A 622GR.A,B,C | 1.1106 | ≤ 16 | 355 |  |  |
|  |  | 16> to ≤35 | 355 |  |  |
|  |  | 35> to ≤50 | 345 |  |  |
|  |  | 50> to ≤70 | 325 | 490-630 | 22 |
|  |  | 70> to ≤100 | 315 | 470-610 | 21 |
|  |  | 100> to ≤150 | 295 | 450-590 | 21 |
|  |  | >150 | 1) | 1) | 1) |

ASTM A622GR.A,B,C impact test:

| Type | Usual Dekivery Condition | Norminal Thickness (mm) | Impact Energy KV min[J] at temperature [°C] |
| --- | --- | --- | --- |
|  |  |  | Longitudinal | Longitudinal |
|  |  |  | -50 | -40 | -20 | 0 | +20 | -50 | -40 | -20 | 0 | +20 |
| A 622GR.A,B,C | N | 5-150 | 30 | 40 | 65 | 90 | 100 | 27 | 30 | 40 | 60 | 70 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.