ASTM A204GRA/B/C steel plate/sheet for boiler steels

Key words:
A204GRA/B/C,steel plate/sheet, ASTM A204GRA/B/C,AMSE SA204GRA/B/C,steel plate/sheet, ASTM A204GRA/B/C steel plate/sheet for boiler steel, A204GRA/B/C carbon steel used for boiler, ASTM ASME steel plate for boiler using, A204GRA/B/C steel supplier/Chinese supplier, A204GRA/B/C steel price, ASTM A204 steel with Cr,Mo used for boiler and pressure vessel

Equivalent grade : 
A204GRA/B/C steel plate/sheet is in ASTM standard. The equal material of A204GRA/B/C is: AFNOR 36206 15CD 2.05

| A204GRA/B/C ASTM | AFNOR 36206 | 15CD 2.05 |
| --- | --- | --- |

ASTM A204GRA/B/C steel Chemical Composition % :

Main chemical composition in ASTM A204GRA/B/C steel : A204GRA Carbon max 0.18,A204GRB Carbon max 0.20,A204GRC Carbon max 0.23;Manganese max 0.90, Silicon  0.15-0.40, Phosphorus max 0.035, Sulphur max 0.035 More detailed information, please refer to the flowing table:

| Grades | C max | Mn max | S max | P max | Si | Cr | Cu | Mo |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A204grA | 0.18 | 0.90 | 0.035 | 0.035 | 0.15-0.40 | - | - | - |
| A204grB | 0.20 | 0.90 | 0.035 | 0.035 | 0.15-0.40 | - | - | - |
| A204grC | 0.23 | 0.90 | 0.035 | 0.035 | 0.15-0.40 | - | - | - |

ASTM A204GRA/B/C steel Mechanical Properties

ASTM A204grA/B/C steel grade is a kind of steel which with Cr., Mo.,Cr-Mo and mainly used for pressure vessels.The steel grade A204grA/B/C is according to ASTM standard which with the yield strength of 242MPa.The followings are the chemical composition and mechanical properties of ASTM A204grA/B/C steel plate. More detailed information about ASTM A204grA/B/C steel Mechanical Properties , please refer to the following table:

| Grade | Tensile Strength (Mpa) | Yield Strength (Mpa) | Elongation in 100-150 mm(%) | Elongation in 16 mm(%) | Max Thickness (mm) |
| --- | --- | --- | --- | --- | --- |
| A204 | 440-590 | 220-275 | 19 | 24 | 250 |

ICE steel is the professional steel exporter in china, We devote extraordinary resources to listening to our customers—to understanding their individual and evolving needs, the characteristics of their markets, and the trends that influence them. Combining insights with innovation, we not only stay in step with our customers, but also keep miles ahead of the competition. we will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.