ASTM A283GrA/B/C/D carbon steel

Key words : 
A283GrA/B/C/D steel plate, ASTM A283GrA/B/C/D steel plate, under ASTM standard, we can regard A283GrA/B/C/D steel plate as Carbon steel
A283GrA/B/C/D steel plate is one mainly of Carbon steel, ASTM A 283A steel covers low and intermediate tensile strength carbon steel plates for general manufacturing and constructional applications. This material is normally supplied in the rimmed or semi-killed types of steel and is particularly suitable for the economical production of assemblies requiring a considerable amount of forming. Variations in low temperature impact properties are great and these steels are not recommended for those applications requiring low temperature notch toughness
Equivalent grade : 
A283GRA/B/C/D steel plate/sheet is in ASTM standard. The equal material of A283GRA/B/C/D is: ASTM:1990 FE 360 B, DIN17100 ST37-2, NFA 35-501 E24-2, JIS3101 SS400 ,UNI7070 FE 360 B .

| A283C ASTM | Comparison of steel grades |
| --- | --- |
|  | ASTM:1990 | FE 360 B |
|  | DIN17100 | ST37-2 |
|  | NFA 35-501 | E24-2 |
|  | JIS3101 | SS400 |
|  | EN 10025-2 | A283GRA/B/C/D |
|  | UNI7070 | FE 360 B |

ASTM A283GRA/B/C/D steel Chemical Composition % : 
 
Main chemical composition in ASTM A283GRA/B/C/D steel : Manganese max 1.4, Phosphorus max 0.045,Sulphur max 0.045. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.17 | 0.20 | -- | 1.40 | 0.045 | 0.045 |

ASTM A283GRA/B/C/D steel Mechanical Properties

ASTM A283GRA/B/C/D steel plate/sheet for carbon steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about ASTM A283GRA/B/C/D steel Mechanical Properties , please refer to the following table:

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 235 225 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 360-510 340-470 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 16 17 18 19 24 |  |

ICE steel is the professional Chinese steel exporter. We can offer you A283GRA/B/C/D sheet, A283GRA/B/C/D Cross Reference, A283GRA/B/C/D Schematic, A283GRA/B/C/D Distributor, A283GRA/B/C/D Equivalent, A283GRA/B/C/D Application Note, A283GRA/B/C/D Data Sheet, A283GRA/B/C/D component, A283GRA/B/C/D Fiche Technique, A283GRA/B/C/D Circuit, A283GRA/B/C/D steel sheet, A283GRA/B/C/D steel price. A283GRA/B/C/D steel supplier, A283GRA/B/C/D steel manufacturer.