ASTM A36 carbon steel
Key words : 
A36 steel plate, ASTM A36 steel plate, under ASTM standard, we can regard A36 steel plate as Carbon steel

ASTM A36 steel Mechanical Properties 
A36 steel plate is one mainly of Carbon steel, ASTM A36 steel is a widely accepted general purpose structural quality steel offering a constant 36 ksi min. yield point for all thicknesses of material. It is widely used in the construction of buildings, bridges and other structures by means of welding, bolting orriveting. This steel is useful because of its wide availability

| Yield point, min. Ksi | up to & incl. 8" thick 36 over 8" thick 32 |
| --- | --- |
| Tensile strength,Ksi | 58-80 |
| Elongation in 8 in., min., % | 20 |
| Elongation in 2 in., min., % | 23 |

ASTM A36 steel Chemical Composition % :  
Main chemical composition in ASTM A36 steel : different thickness with different chemical composition. More detailed information, please refer to the flowing table:

| Thickness, in | All | To 3⁄4 | Over | Over | Over 5⁄2to4incl. | Over |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 3⁄4to3⁄2incl. | 3⁄2to5⁄2incl. |  | 4 |
| Carbon, max, % | 0.26 | 0.25 | 0.25 | 0.26 | 0.27 | 0.29 |
| Manganese, % | - | - | 0.80-1.20 | 0.80-1.20 | 0.85-1.20 | 0.85-1.20 |
| Phosphorus, max, % | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 |
| Sulfur, max, % | 0.05 | 0.05 | 0.05 | 0.05 | 0.05 | 0.05 |
| Silicon, % | - | 0.40 | 0.40 | 0.15-0.40 | 0.15-0.40 | 0.15-0.40 |
| Copper, min, % | 0.20 | 0.20 | 0.20 | 0.20 | 0.20 | 0.20 |

ICE steel is the professional Chinese steel exporter. We can offer you A36 sheet, A36 Cross Reference, A36 Schematic, A36 Distributor, A36 Equivalent, A36 Application Note, A36 Data Sheet, A36 component, A36 Fiche Technique, A36 Circuit, A36 steel sheet, A36 steel price. A36 steel supplier, A36 steel manufacturer.