ASTM A515gr.55, 60, 65, 70 Boiler Pressure Vessel

Key words :

A515gr.55,60,65,70 steel plate, ASTM A515gr.55,60,65,70 steel plates is a kind of material for boiler and pressure vessel steel. ASTM A515gr.55,60,65,70 steel plates is characterized by a minimum yield strength of 220 - 295 MPa and by good weldability, so A515gr.55,60,65,70 steel is mainly used to for manufacturing boilers, pressure vessels and pipes transporting hot liquids. the following are ASTM A515gr.55,60,65,70 steel plate's Chemical composition and mechanical properties.

If you are looking for Chinese A515gr.55, 60, 65, 70 steel supplier, if you want to know A515gr.55,60,65,70 steel price, please be free to contact us. 

ASTM A515gr.55,60,65,70 steel Chemical Composition % : 
Main chemical composition in ASTM A515gr.55,60,65,70 steel: Carbon from 0.08 to 0.2, Manganese from 0.90 to 1.50, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.40, More detailed information, please refer to the flowing table:

| Grade | C. % | Mn.% | S. | N | Cu | Nb | Ti. | Si. | P. | AL | Cr. | Mo. | Ni | Vi |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A515gr.55,60,65,70 | 0.08-0.2 | 0.90-1.50 | 0.015 | 0.012 | 0.30 | 0.020 | 0.03 | 0.40 | 0.025 | 0.020 | 0.30 | 0.08 | 0.30 | 0.02 |

ASTM A515gr.55,60,65,70 steel Mechanical Properties 
A515gr.55,60,65,70 this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 220- 295 MPa (there is different min strength point at the different thickness.) A515gr.55,60,65,70 tensile strength is from 430MPa to 580MPa. (different min strength point at the different thickness.) More detailed information about ASTM A515gr.55,60,65,70 steel Mechanical Properties , please refer to the following table:

| Grade | Type | Thickness mm | Yield strength Mpa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KVJ) (min) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -20° | 0° | +20 |
| A515gr.55,60,65,70 | Normalized | ≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250 | 295 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 290 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 285 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 260 | 460-580 | 21 | 27 | 34 | 40 |
|  |  |  | 235 | 440-570 | 21 | 27 | 34 | 40 |
|  |  |  | 220 | 430-570 | 21 | 27 | 34 | 40 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.