ASTM A516Gr55 Weldable normalized fine grained pressure vessel steels
Key words :
ASTM A516Gr55 steel plate/sheet,ASTM A516Gr55 steel plate/sheet, under ASTM standard, we can regard A516Gr55 steel plate/sheet for simple pressure vessels steel.

A516 Grade 55 steel grade is used in moderate and lower temperature pressure vessels steel because of the steel material chemical composition and the property in welding.For the reason of excellent notch toughness and weldability of A516 Grade 55, it sells good to large fabricators service in gas & oil plants.The followings are the chemical composition and mechanical properties of ASTM A516Gr.55 steel plate sheet.

ASTM A516Gr55 steel Chemical Composition % : 
Main chemical composition in ASTM A516Gr55 steel: Carbon from 0.18 to 0.26, Manganese from 0.55-1.3, Sulphur max 0.035, Phosphorus max 0.035, Silicon max 0.13-0.45, More detailed information, please refer to the flowing table:

| Grade | C | Si | Mn | P | S |
| --- | --- | --- | --- | --- | --- |
| A516Gr.55 | 0.18-0.26 | 0.13-0.45 | 0.55-1.3 | 0.035 | 0.035 |

ASTM A516Gr55 steel Mechanical Properties 
A516Gr55 this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 380-515 MPa (there is different min strength point at the different thickness.) A516Gr55 tensile strength is 205MPa. (different min strength point at the different thickness.) More detailed information about ASTM A516Gr55 steel Mechanical Properties , please refer to the following table:

| Grade | Thickness (mm) | Tensile strength [MPa] | Yield strength Min.[MPa] | Elongation [%] |
| --- | --- | --- | --- | --- |
| A516Gr.55 | 6-40 | 205 | 380-515 | 27 |
|  | 40-100 | 205 | 380-515 | 23 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.