ASTM A516Gr65 Weldable normalized fine grained pressure vessel steels
Key words :
ASTM A516Gr65 steel plate/sheet,ASTM A516Gr65 steel plate/sheet, under ASTM standard, we can regard A516Gr65 steel plate/sheet for simple pressure vessels steel.

ASTM A516Gr65/ASME SA516Gr65 is an excellent weldable carbon steel choice for pressure vessels and boiler fabrication. The material offers excellent performance in lower than ambient temperature service, has good weldability and excellent notch toughness.

ASTM A516 Grade 65/ASME SA516 Grade65A has greater specified tensile and yield strength when compared with ASTM A516 Gr60/ASME SA516Gr60.

ASTM A516Gr65 steel Chemical Composition % : 
Main chemical composition in ASTM A516Gr65 steel: Carbon from 0.24 to 0.29, Manganese from 0.85 to 1.30, Sulphur max 0.035, Phosphorus max 0.035, Silicon max 0.15-0.40, More detailed information, please refer to the flowing table:

| Carbon(C) | % | Manganese(Mn) | % | Phosphorus(P) | % |
| --- | --- | --- | --- | --- | --- |
| 12.55mm or less 12.5-50mm 50-100mm 100-200mm >200mm | 0.24 0.26 0.28 0.29 0.29 | 12.5mm or less Heat Analysis Product Analysis Over 12.5mm Heat Analysis Product Analysis | 0.85-1.20 0.79-1.30 0.85-1.20 0.79-1.30 | (max) | 0.035 |
| Sulphur(S) | % | Silicon(Si) | % |  |
| (max) | 0.035 | Heat Analysis Product Analysis | 0.15-0.40 0.13-0.45 |  |

ASTM A516Gr65 steel Mechanical Properties

ASTM A516Gr65 steel plate/sheet for carbon and low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about ASTM A516Gr65 steel Mechanical Properties , please refer to the following table:

| Description | Grade65 |
| --- | --- |
| Tensile Strength(Ksi) Tensile Strength(MPa) Yield Strength(Ksi) Elongation in 200mm(min.%) Elongation in 50mm(min.%) Thickness(max/min) | 65-85 450-585 35 240 19 21 205 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.