ASTM A516Gr70 Weldable normalized fine grained pressure vessel steels
Key words :
ASTM A516Gr70 steel plate/sheet,ASTM A516Gr70 steel plate/sheet, under ASTM standard, we can regard A516Gr70 steel plate/sheet for simple pressure vessels steel.

ASTM A516Gr70/ASME SA516Gr70 is an excellent choice for service in lower than ambient temperature applications, has excellent notch toughness and is used in both pressure vessels and industrial boilers.ASTM A516Gr70/ASME SA516Gr70 offers greater tensile and yield strength when compared to ASTM A516Gr65/ASME SA516Gr65 and can operate in even lower temperature service.

ASTM A516Gr70 steel Chemical Composition % : 
Main chemical composition in ASTM A516Gr70 steel: Carbon from 0.27 to 0.31, Manganese from 0.85 to 1.30, Sulphur max 0.035, Phosphorus max 0.035, Silicon max 0.15-0.40, More detailed information, please refer to the flowing table:

| Carbon(C) | % | Manganese(Mn) | % | Phosphorus(P) | % |
| --- | --- | --- | --- | --- | --- |
| 12.55mm or less 12.5-50mm 50-100mm 100-200mm >200mm | 0.27 0.28 0.30 0.31 0.31 | 12.5mm or less Heat Analysis Product Analysis Over 12.5mm Heat Analysis Product Analysis | 0.85-1.20 0.79-1.30 0.85-1.20 0.79-1.30 | (max) | 0.035 |
| Sulphur(S) | % | Silicon(Si) | % |  |
| (max) | 0.035 | Heat Analysis Product Analysis | 0.15-0.40 0.13-0.45 |  |

ASTM A516Gr70 steel Mechanical Properties

ASTM A516Gr70 steel plate/sheet for carbon and low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about ASTM A516Gr70 steel Mechanical Properties , please refer to the following table:

| Description | Grade70 |
| --- | --- |
| Tensile Strength(Ksi) Tensile Strength(MPa) Yield Strength(Ksi) Elongation in 200mm(min.%) Elongation in 50mm(min.%) Thickness(max/min) | 70-79 485-620 38 260 17 21 205 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.