ASTM A537 CL2 Weldable normalized fine grained pressure vessel steels
Key words : 
ASTM A537 CL2 steel plate/sheet,ASTM A537 CL2 steel plate/sheet, under ASTM standard, we can regard A537 CL2 steel plate/sheet for simple pressure vessels steel.

A 537 Class 2carbon steel plates are engineered to be used in pressure vessel applications.ASTM A537 Class 2 steel is a higher yield and tensile strength material used in the fabrication of pressurised vessels and steel boilers. he steel includes the alloying of carbon, manganese and silicon and is heat treated using the quenched and tempered method which gives the material its residual strength. Sourced by the world's leading fabricators, ASTM A537 Class 2 is a material used extensively by the oil, gas and petrochemical industry.

ASTM A537 CL2 steel Chemical Composition % : 
Main chemical composition in ASTM A537 CL2 steel: Carbon max 0.24, Manganese from 0.7-1.6, Sulphur max 0.035, Phosphorus max 0.035, Silicon from 0.15-0.5, More detailed information, please refer to the flowing table:

| Grade | C | Si | Mn | P | S | Cr | Mo | Ni | Cu |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | ≤40 mm | >40 mm |  |  |  |  |  |  |
| A537CL2 | 0.24 | 0.15- 0.50 | 0.70- 1.35 | 1.00- 1.60 | 0.035 | 0.035 | 0.25 | 0.80 | 0.25 | 0.35 |

ASTM A537 CL2 steel Mechanical Properties 
A537 CL2 this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 315- 415 MPa (there is different min strength point at the different thickness.) A537 CL2 tensile strength is from 485MPa to 690MPa. (different min strength point at the different thickness.) More detailed information about ASTM A537 CL2 steel Mechanical Properties , please refer to the following table:

| Grade | Yield strength (MPa) | Tensile strength (MPa) | Elongation | Thickness |
| --- | --- | --- | --- | --- |
|  |  |  | A50mm | A200mm |  |
| A537 CL2 | 415 | 550-690 | 22% | - | ≤65 |
|  | 380 | 515-655 | 22% | - | >65≤100 |
|  | 315 | 485-620 | 20% | - | >100≤150 |

BeiJing ICE Iron &steel CO.,Ltd Will return you with high-quality products and complete after-sale service with the lowest price. we committed to exceed customer’s expectation on the basis of quality, price, and delivery. We sincerely hope to establish long-term cooperation relationship with you on the basis of mutual benefit, reciprocity and common development.