ASTM A572Gr42/50 low alloy steels
Key words : 
A572Gr42/50 steel plate, ASTM A572Gr42/50 steel plate, under ASTM standard, we can regard A572Gr42/50 steel plate as low alloy steel
A572Gr42/50 steel plate is one mainly of low alloy steel, ASTM A572Gr42,50,55,60,65 steel is high strength low alloy steel plate sheet which is widely used  in plants building, general mansions and all kinds of construction machinery, such as mines and various types of drilling rig used in construction, power shovel, electric wheel dump trucks, mining vehicles,excavators, loaders, bulldozers , various types of cranes, hydraulic support, coal mining machinery and equipments and other structures 
Equivalent grade : 
A572Gr42/50 steel plate/sheet is in ASTM standard.The equal material of A572Gr42/50 is: ASTM:1990 FE 510 B, DIN17100 ST52-3, NFA 35-501 E36-2, EN 10025-2 S355JR, JIS SS490/SM490A, BS1449 50B,UNI7070 FE 510 B .

| A572GR50 ASTM | Comparison of steel grades |
| --- | --- |
|  | ASTM:1990 | FE 510 B |
|  | DIN17100 | ST52-3 |
|  | EN 10025-2 | S355JR |
|  | JIS | SS490/SM490A |
|  | NFA 35-501 | E36-2 |
|  | BS1449 | 50B |
|  | UNI7070 | FE 510 B |

ASTM A572Gr42/50 steel Chemical Composition % : 
 
Main chemical composition in ASTM A572Gr42/50 steel : Silicium max 0.55,Manganese max 1.6, Phosphorus max 0.045,Sulphur max 0.045. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.24 | 0.24 | 0.55 | 1.60 | 0.045 | 0.045 |

ASTM A572Gr42/50 steel Mechanical Properties

ASTM A572Gr42/50 steel plate/sheet for low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about ASTM A572Gr42/50 steel Mechanical Properties , please refer to the following table:

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |

ICE steel is the professional Chinese steel exporter. We can offer you A572Gr42/50 sheet, A572Gr42/50 Cross Reference, A572Gr42/50 Schematic, A572Gr42/50 Distributor, A572Gr42/50 Equivalent, A572Gr42/50 Application Note, A572Gr42/50 Data Sheet, A572Gr42/50 component, A572Gr42/50 Fiche Technique, A572Gr42/50 Circuit, A572Gr42/50 steel sheet, A572Gr42/50 steel price. A572Gr42/50 steel supplier, A572Gr42/50 steel manufacturer.