ASTM -SAE SAE 1008 steel plate/sheet for stamping and cold forming steels
ASTM SAE 1008 steel plate/sheet,SAE 1008 steel plate/sheet, under EN standard, ASTM-SAE SAE 1008 steel plate/sheet for stamping and cold forming steels,A 621 DQ - SAE 1008 steel supplier/Chinese supplier, A 621 DQ - SAE 1008 steel price,SAE 1008 steel manufacturer.

SAE 1008 steel plate/sheet is in ASTM-SAE standard. It's grade Number is 1.0398. The equal material of SAE 1008 is: DIN 1614 RRSTW23,EN 10111 DD12,JIS G 3131 SPHE.

| SAE 1008 JIS G 3131 Number: 1.0398 | Comparison of steel grades |
| --- | --- |
|  | UNI5867 | - |
|  | DIN1614 | RRSTW23 |
|  | NFA 36-301 | - |
|  | EN 10111 | DD12 |
|  | ASTM-SAE | A621DQ-SAE1008 |
|  | UNE36.093 | - |

Main chemical composition in ASTM-SAE A 621 DQ - SAE 1008 steel: Carbon max 0.10, Manganese max 0.45,Phosphorus max 0.035, Sulphur max 0.035,More detailed information,please refer to the flowing table: 
Chemical analysis -% by mass*

| Chemical elements | C | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- |
| SAE 1008 | 0.10 | -- | 0.45 | 0.035 | 0.035 |

ASTM-SAE SAE 1008 steel plate/sheet is stamping and cold forming steels,it is suitable for non-structural press work and forming.It's yield strength is between 170 to 320 MPa (there is different min strength point at the different thickness.) A 621 DQ - SAE 1008 tensile strength is from around 420 MPa. (different min strength point at the different thickness.) More detailed information about ASTM-SAE SAE 1008 steel Mechanical Properties , please refer to the following table: 
Mechanical properties

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Bending Test transv.bending mandrel Ø angle = 180° s = plate thickness |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 170-320 |  |  | 0 S |
| t < 3mm t ≥ 3mm |  | 420 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 25 A80 26 A80 30 A5 |  |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like ASTM-SAE SAE 1008 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products ASTM-SAE A 621 DQ - SAE 1008 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.