ASTM - SAE A 621 CQ - SAE 1010 steel plate/sheet for stamping and cold forming steels
ASTM - SAE 1010 steel plate/sheet,A 621 CQ - SAE 1010 steel plate/sheet, under EN standard, ASTM - SAE A 621 CQ - SAE 1010 steel plate/sheet for stamping and cold forming steels,A 621 CQ - SAE 1010 steel supplier/Chinese supplier,SAE 1010 steel price,A 621 CQ - SAE 1010 steel manufacturer.

SAE 1010 steel plate/sheet is in ASTM - SAE standard. It's grade Number is 1.0332. The equal material of A 621 CQ - SAE 1010 is: DIN 1614 STW22, NFA 36-301 1C, UNI5867 FEP11, BS1449 HR3,UNE36.093  AP11, EN 10111 DD11,JIS G 3131 SPHD.

| A 621 CQ - SAE 1010 ASTM - SAE Number: 1.0332 | Comparison of steel grades |
| --- | --- |
|  | UNI5867 | FEP11 |
|  | DIN1614 | STW22 |
|  | NFA 36-301 | 1C |
|  | JIS G 3131 | SPHD |
|  | EN 10111 | DD11 |
|  | BS1449 | HR3 |
|  | UNE36.093 | AP11 |

Main chemical composition in ASTM - SAE 1010 steel: Carbon:max 0.20, Manganese max 0.60, Sulphur max 0.045, Phosphorus max 0.045. More detailed information, please refer to the flowing table: 
Chemical analysis -% by mass*

| Chemical elements | C | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- |
| SAE 1010 | 0.12 | -- | 0.60 | 0.045 | 0.045 |

ASTM - SAE A 621 CQ - SAE 1010 steel plate/sheet is stamping and cold forming steels,it is suitable for non-structural press work and forming.It's tensile strength is around 420 MPa (there is different min strength point at the different thickness.) A 621 CQ - SAE 1010 yield strength is from 170MPa to 320 MPa. (different min strength point at the different thickness.) More detailed information about ASTM SAE 1010 steel Mechanical Properties , please refer to the following table:
Mechanical properties

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Bending Test transv.bending mandrel Ø angle = 180° s = plate thickness |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 170-340 |  |  | 1 S |
| t < 3mm t ≥ 3mm |  | 440 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 23 A80 24 A80 28 A5 |  |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like ASTM - SAE A 621 CQ - SAE 1010 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products ASTM - SAE A 621 CQ - SAE 1010 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.