Key words: 43 EE steel plate/sheet, BS 1449 43 EE steel plate/sheet, BS 1449 43 EE steel plate/sheet supplier/Chinese supplier, 43 EE steel plate/sheet mechanical property, 43 EE steel plate/sheet price.
BS 1449 43 EE steel equivalent grade:
43 EE steel plate/sheet is in BS 1449 standard, the grade number is 1.0491. The equivalent material of 43 EE steel are UNE36081 AE285KG/AE285KW, DIN1614/2 S275N, UN Fe E 275KG N.

| 43EE BS1449 MATERIAL# 1.0491 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE285KG/AE285KW |
|  | DIN1614/2 | S275N |
|  | NFA 36-301 | - |
|  | UN | Fe E 275KG N |

BS 1449 43 EE steel chemical composition %:
Main chemical composition in 43 EE steel is carton max 0.18, silicon max 0.40, manganese max 0.50-1.50, phosphorus max 0.03, Sulphur max 0.025, chromium max 0.30. More detailed information about 43 EE steel, please refer to the down table:

| Chemical elements | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.18 | 0.40 | 0.50-1.50 | 0.030 | 0.025 | 0.55 | 0.30 | 0.30 | 0.05 | 0.05 | 0.02 |

BS 1449 43 EE steel mechanical property:
43EE steel plate is one mainly of Fine-grain structural steels, normalised rolled steel,43EE steel plate is under BS1449 standard equivalent to DIN:43EE,which with a minimum impact energy of 20J at temperatures not lower than -20 degree and the tensile strength of 43EE is 370 to 510MPa.

| thickness | Yield Strength ReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 275 265 |  |  | +20 KV 31J 0 KV 27J -10 KV 24J -20 KV 20J -40 - -50 - |
| t < 3mm t ≥ 3mm |  | 370-510 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 24 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of BS 1449 43 EE steel are available, so if need, welcome to contact ICE steel sales team.