Key words: 50 EE steel plate/sheet, BS 1449 50 EE steel plate/sheet, BS 1449 50 EE steel plate/sheet supplier/Chinese supplier, 50 EE steel plate/sheet mechanical property, 50 EE steel plate/sheet price.
BS 1449 50 EE steel equivalent grade:
50 EE steel plate/sheet is in BS 1449 standard, the grade number is 1.0546. The equivalent material of 50 EE steel are SEW 083 TStE 460 TM, NFA 36-201 E 460 FP, UNI 7382 Fe E 460 KGTM, EN10113-3 S460ML, ASTM A 572 Gr.65.

| 55EE BS 1449 Number:1.0546 | Comparision of steel grades |
| --- | --- |
|  | SEW 083 | TStE 460 TM |
|  | NFA 36-201 | E 460 FP |
|  | UNI 7382 | Fe E 460 KGTM |
|  | EN10113-3 | S460ML |
|  | ASTM | A 572 Gr.65 |

BS 1449 50 EE steel chemical composition %:
Main chemical composition in 50 EE steel is carton max 0.16, silicon max 0.60, manganese max 1.70, phosphorus max 0.025, Sulphur max 0.02, chromium max 0.30. More detailed information about 50 EE steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BS 144955EE | 0.16 | 0.60 | 1.70 | 0.025 | 0.02 | 0.025 | 0.02 | 0.05 | 0.12 | 0.05 | 0.30 | 0.80 | 0.20 | 0.55 | 0.48 |

BS 1449 50 EE steel mechanical property:
BS 1449 55EE is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy at temperature not lower than -50 degree.

| Temperature | -50 | -40 | -30 | -20 | -10 | 0 | 20 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 27 | 31 | 40 | 47 | 51 | 55 | 63 |
| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| ReH-Minimun yield strength(Mpa) | 460 | 440 | 430 | 410 | 400 | 385 |
| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| Rm-Tensile strength(Mpa) | 540-720 | 530-710 | 510-690 | 500-680 | 490-660 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 17 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of BS 1449 50 EE steel are available, so if need, welcome to contact ICE steel sales team.