Key words: TStE 285 steel plate/sheet, DIN 1614/2 TStE 285 steel plate/sheet, TStE 285 steel plate/sheet supplier/Chinese supplier, TStE 285 steel plate/sheet mechanical property, TStE 285 steel plate/sheet price.
DIN 1614/2 TStE 285 steel equivalent grade:
TStE 285 steel plate/sheet is in DIN 1614/2 standard, the grade number is 1.0491. The equivalent materials of TStE 285 steel are UNE36081 AE 285 KT, EN 10025-3 S275NL, UN Fe E 275 KT N, BS4360 43 EE.

| T StE 285 DIN1614/2 MATERIAL# 1.0491 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE 285 KT |
|  | EN 10025-3 | S275NL |
|  | UN | Fe E 275 KT N |
|  | BS4360 | 43 EE |

DIN 1614/2 TStE 285 steel chemical composition %:
Main chemical composition in TStE 285 steel is carton max 0.16, silicon max 0.40, manganese max 0.50-1.50, phosphorus max 0.025, Sulphur max 0.020, chromium max 0.30. More detailed information about TStE 285 steel, please refer to the down table:

| Chemical elements | C max | Si max | Mn max | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TStE285 | 0.16 | 0.40 | 0.50-1.50 | 0.025 | 0.020 | 0.55 | 0.30 | 0.30 | 0.05 | 0.05 | 0.02 |

DIN 1614/2 TStE 285 steel mechanical property:
DIN 171022 TStE 285 steel plate/sheet is a hot rolled structural steels, which technical delivery conditions for normalized or normalized rolled in weldable fine grain structural steel grade.