Key words: StE 420 steel plate/sheet, DIN 1614/2 StE 420 steel plate/sheet, StE 420 steel plate/sheet supplier/Chinese supplier, StE 420 steel plate/sheet mechanical property, StE 420 steel plate/sheet price.
DIN 1614/2 StE 420 steel equivalent grade:
StE 420 steel plate/sheet is in DIN 1614/2 standard, the grade number is 1.8902. The equivalent materials of StE 420 steel are UNE36081 AE420KG/AE420KW, EN 10111 S420N, NFA 36-201 E420R.

| STE420 DIN1614/2 MATERIAL#1.8902 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE420KG/AE420KW |
|  | EN 10111 | S420N |
|  | NFA 36-201 | E420R |
|  | BS4036 | - |
|  | UN | - |

DIN 1614/2 StE 420 steel chemical composition %:
Main chemical composition in StE 420 steel is carton max 0.20, silicon max 0.60, manganese max 1.00-1.70, phosphorus max 0.030, Sulphur max 0.025, chromium max 0.30. More detailed information about StE 420steel, please refer to the down table:

| Chemical elements | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.60 | 1.00-1.70 | 0.030 | 0.025 | 0.55 | 0.30 | 0.50 | 0.12 | 0.05 | 0.02 |

DIN 1614/2 StE 420 steel mechanical property:
StE420steel plate is one mainly of Fine-grain structural steels, normalised rolled steel, which with a minimum elongation of 19%

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 420 400 |  |  | +20 KV 31J 0 KV 27J -10 KV 24J -20 KV 20J -40 - -50 - |
| t < 3mm t≥ 3mm |  | 520-680 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 19 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of DIN 1614/2 StE 420 steel are available, so if need, welcome to contact ICE steel sales team.