DIN 17102 E St E 460 steel plate/sheet for High Yield Steel

Key words: E STE 460 steel plate/sheet, DIN 17102 E STE 460 steel plate/sheet, E STE 460 steel plate/sheet supplier/Chinese supplier, E STE 460 steel plate/sheet price, E STE 460 steel plate/sheet mechanical property.

DIN 17102 E STE 460 steel chemical composition %:
Main chemical composition in DIN 17102 E STE 460 steel is carton max 0.20, silicon max 0.60, manganese max 1.70, phosphorus max 0.020, Sulphur max 0.010. More detailed information about E STE 460 steel, please refer to the down table:

| Element | E St E 460 | Element | E St E 460 |
| --- | --- | --- | --- |
| Carbon max. | 0.20 | Silicon max. | 0.60 |
| Manganese | 1.10 to 1.70 | Phosphorous max. | 0.020 |
| Sulphur max. | 0.010 | Chromium min. | 0.30 |
| Molybdenum max. | 0.10 | Nickel max. | 0.80 |
| Niobium max. | 0.05 | Titanium max. | 0.03 |
| Vanadium max. | 0.20 | Nitrogen max. | 0.025 |
| Aluminium max. | 0.020 | Copper max. | 0.70 |

DIN 17102 E STE 460 steel mechanical property:
E St E 460 steel plate is one of the mainly High Yield steel, Steel sheet E St E 460 Boiler steel plates P460Nl1 tensile strength is at 570_720 Mpa for thickness belows 60mm,even maximum 730 Mpa is OK for the product thicknesses up to 16 millimeters.

| Grade | Type | Thickness (mm) | Yield Strength MPa (min) | Tensile Strength MPa | Elongation % (min) |
| --- | --- | --- | --- | --- | --- |
| E St E 460 | Normalized | ≤ 16 16> to ≤40 40> to ≤60 60> to ≤100 100> to ≤150 | 460 445 430 400 – | 570 to 750 570 to 720 570 to 720 540 to 710 – | 17 17 17 17 17 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of DIN 17102 E STE 460 steel are available, so if need, welcome to contact ICE steel sales team.