DIN 17102 STE 380 steel plate/sheet for High Yield Steel

Key words: STE 380 steel plate/sheet, DIN 17102 STE 380 steel plate/sheet, STE 380 steel plate/sheet supplier/Chinese supplier, STE 380 steel plate/sheet price, STE 380 steel plate/sheet mechanical property.

DIN 17102 STE 380 steel equivalent grade:
STE 380 steel plate/sheet is in DIN 17102 standard, the equivalent grade of STE 380 steel are NFA 36201 E 375R, MNC 810E SS21,42,01, CSA G40-21 400 W, WT, JIS 3101 SS 540, ASTM A 572gr. 60,65.

| STE 380 DIN 17102 | Comparision of steel grades |
| --- | --- |
|  | NFA 36201 | E 375R |
|  | MNC 810E | SS21,42,01 |
|  | CSA G40-21 | 400 W, WT |
|  | JIS 3101 | SS 540 |
|  | ASTM | A 572gr. 60,65 |

DIN 17102 STE 380 steel chemical composition %:
Main chemical composition in DIN 17102 STE 380 steel is carton max 0.26, silicon max 0.40, manganese max 1.35, phosphorus max 0.04, Sulphur max 0.05. More detailed information about STE 380 steel, please refer to the down table:

| Symbol | Chemical composition |
| --- | --- |
|  | C max | Si max | Mn max | P max | S max |
| Grade60 | 0.26 | 0.40 | 1.35 | 0.04 | 0.05 |
| Grade65 | 0.26 | 0.40 | 1.35 | 0.04 | 0.05 |

DIN 17102 STE 380 steel mechanical property:
STE 380 steel plate is one mainly of High Yield steel, DIN 17102 STE 380is high strength low alloy steel plate sheet which is widely used in plants building, general mansions and all kinds of construction machinery, such as mines and various types of drilling rig used in construction, power shovel, electric wheel dump trucks, mining vehicles, excavators, loaders, bulldozers, various types of cranes, hydraulic support, coal mining machinery and equipments and other structures.

| Symbol | Yield point min MPa | Tensile strength MPa | Elongation in 2 in.(50mm)% |
| --- | --- | --- | --- |
| Grade A | 165 | 310-450 | 30 min |
| Grade B | 185 | 345-450 | 28 min |
| Grade C | 205 | 380-515 | 25 min |
| Grade D | 230 | 415-550 | 23 min |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of DIN 17102 STE 380 steel are available, so if need, welcome to contact ICE steel sales team.