DIN 17102 T St E 460 steel plate/sheet for High Yield Steel

Key words: T STE 460 steel plate/sheet, DIN 17102 T STE 460 steel plate/sheet, T STE 460 steel plate/sheet supplier/Chinese supplier, T STE 460 steel plate/sheet price, T STE 460 steel plate/sheet mechanical property.

DIN 17102 T STE 460 steel chemical composition %:
Main chemical composition in DIN 17102 T STE 460 steel is carton max 0.20, silicon max 0.60, manganese max 1.70, phosphorus max 0.025, Sulphur max 0.015. More detailed information about T STE 460 steel, please refer to the down table:

| Element | P460NL1 | Element | P460NL1 |
| --- | --- | --- | --- |
| Carbon (C) max. | 0.20 | Silicon (Si) max. | 0.60 |
| Manganese (Mn) | 1.10 to 1.70 | Phosphorous (P) max. | 0.025 |
| Sulphur (S) max. | 0.015 | Chromium (Cr) min. | 0.30 |
| Molybdenum (Mo) max. | 0.10 | Nickel (Ni) max. | 0.80 |
| Niobium (Nb) max. | 0.05 | Titanium (Ti) max. | 0.03 |
| Vanadium (V) max. | 0.20 | Nitrogen (N) max. | 0.025 |
| Aluminium (Al) max. | 0.020 | Copper (Cu) max. | 0.70 |

DIN 17102 T STE 460 steel mechanical property:
TSt E 460 steel plate is one of the mainly High Yield steel, Steel sheet TSt E 460 Boiler steel plates TSt E 460 tensile strength is at 570_720 Mpa for thickness belows 60mm,even maximum 730 Mpa is OK for the product thicknesses up to 16 millimeters.

| Grade | Type | Thickness (mm) | Yield Strength MPa (min) | Tensile Strength MPa | Elongation % (min) |
| --- | --- | --- | --- | --- | --- |
| TSt E 460 | Normalized | ≤ 16 16> to ≤40 40> to ≤60 60> to ≤100 100> to ≤150 | 460 445 430 400 – | 570 to 750 570 to 720 570 to 720 540 to 710 – | 17 17 17 17 17 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of DIN 17102 T STE 460 steel are available, so if need, welcome to contact ICE steel sales team.