DIN 17155 15Mo3 steel plate/sheet for Boiler and Pressure Vessel

15Mo3 steel plate/sheet, 15Mo3 steel plate/sheet metal, DIN 17155 15Mo3 steel plate/sheet for boiler steel, 15Mo3 carbon steel used for boiler, DIN 17155 steel plate for boiler using, 15Mo3 steel supplier/Chinese supplier, 15Mo3 steel price,15Mo3 steel manufacturer.

15Mo3 steel plate/sheet is one mainly of Steel for boiler steels.DIN 17155 15Mo3 steel is mainly used for boilers and pressure vessels with elevated temperatures which is equivalent to EN10028 16Mo3 and UNI5869 15Mo3, 15D3 (NFA 36205 ) and ASTM A204Gr.B.

| 15Mo3 DIN 17155 Number:1.5415 | Comparison of steel grades |
| --- | --- |
|  | EN 10028-2 | 16 Mo 3 |
|  | NFA 36-205 | 15 D3 |
|  | UNI 5869 | 15 Mo 3 |
|  | BS 1501 | 1503 - 243 B |
|  | UNE 36087 | 16 Mo 3 |
|  | ASTM | A 204 Gr. B |
|  | JIS G3115 | - |

Main chemical composition in DIN 17155 15Mo3 steel : Carbon from 0.12 to 0.20, Manganese from 0.40 to 0.90, Sulphur max 0.01, Phosphorus max 0.025, Silicon max 0.350,Molybdenum from 0.25 to 0.35, Chromium max 0.30.More detailed information, please refer to the flowing table:

| Grade | C. max | Mn. | S. | N | Cu | Si. | P. | Cr. | Ni. | Mo. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 15Mo3 | 0.12- 0.2 | 0.40- 0.90 | 0.01 | 0.012 | 0.30 | 0.35 | 0.025 | 0.30 | 0.30 | 0.25- 0.35 |

15Mo3 material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and mechanical properties. It's yield strength is from 220 to 275 MPa.15Mo3 tensile strength is from 440 MPa to 590 MPa.More detailed information about DIN 17155 15Mo3 steel Mechanical Properties , please refer to the following table:

| Grade | Tensile Strength (Mpa) | Yield Strength (Mpa) | Elongation in 100-150 mm(%) | Elongation in 16 mm(%) | Max Thickness (mm) |
| --- | --- | --- | --- | --- | --- |
| 15Mo3 | 440-590 | 220-275 | 19 | 24 | 250 |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.