DIN 17155 19Mn6 steel plate/sheet for Boiler and Pressure Vessel

19Mn6 steel plate/sheet, 19Mn6 steel plate/sheet metal, DIN 17155 19Mn6 steel plate/sheet for boiler steel, 19Mn6 carbon steel used for boiler, DIN 17155 steel plate for boiler using, 19Mn6 steel supplier/Chinese supplier, 19Mn6 steel price,19Mn6 steel manufacturer.

19Mn6 steel plate/sheet is in DIN 17155 standard. It's grade Number is 1.0557. The equal material of 19Mn6 is:NFA 36-211 BS6,BS 5045 Type E,UNI 7355 FeE35KR,EN10120  P355NB,JIS G3116  SG 365.

| 19Mn6 DIN17155 Material no.1.0557 | Comparison of steel grades |
| --- | --- |
|  | EN10120 | P355NB |
|  | NFA36-211 | BS6 |
|  | UNI7355 | FeE35KR |
|  | BS5045 | Type E |
|  | JIS G3116 | SG 365 |

Main chemical composition in DIN 17155 19Mn6 steel : Carbon max 0.20 , Manganese max 0.7, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.50, More detailed information, please refer to the flowing table:

| Grades | C max | Si max | Mn. max | P max | S max | N max | AL min | Nb max | Ti max | V max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 19Mn6 | 0.2 | 0.5 | 0.7 | 0.025 | 0.015 | 0.009 | 0.02 | 0.05 | 0.03 | - |

19Mn6 material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and mechanical properties. It's yield strength is around 355 MPa.19Mn6 tensile strength is from 510 MPa to 620 MPa. (different min strength point at the different thickness.) More detailed information about DIN 17155 19Mn6 steel Mechanical Properties , please refer to the following table:

| Grades | Yield Strength ReH[N/mm2] transv.min. | Tensile Strength Rm[N/mm2]transv. | Fracture Elongation [%]transv. min. |
| --- | --- | --- | --- |
| 19Mn6 |  |  |  |
|  |  |  | thickness | Total elongation A1 |
|  |  |  | < 3 mm | ≥ 19% |
|  | 355 | 510 - 620 | ≥ 3 mm | ≥ 24% |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.