DIN 17155 HII steel plate/sheet for Boiler and Pressure Vessel

HII steel plate/sheet, HII steel plate/sheet metal, DIN 17155 HII steel plate/sheet for boiler steel, HII carbon steel used for boiler, DIN 17155 steel plate for boiler using, HII steel supplier/Chinese supplier, HII steel price,HII steel manufacturer.

HII steel plate/sheet is in DIN 17155 standard. It's grade Number is 1.0425. The equal material of HII is:NFA 36-205 A 42 CP,UNE 36087 A 42 RCI, BS 1501 161 Gr.400/164 Gr.400/224 Gr. 400,UNI 5869 Fe 410-1KW,EN 10028-2 P265GH.

| HII DIN 17155 Number:1.0425 | Comparison of steel grades |
| --- | --- |
|  | EN 10028-2 | P265GH |
|  | NFA 36-205 | A 42 CP |
|  | UNI 5869 | Fe 410-1KW |
|  | BS 1501 | 161 Gr.400/164 Gr.400/224 Gr. 400 |
|  | UNE 36087 | A 42 RCI |
|  | ASTM | A 414 Gr. E / A 516 Gr. 60 |
|  | JIS G3115 | - |

Main chemical composition in DIN 17155 HII steel : Carbon max 0.20 , Manganese from 0.80 to 1.40, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.40, More detailed information, please refer to the flowing table:

| Grade | C. % | Mn. % | S. max | N | Cu | Nb | Ti. max | Si. | P. max | AL. | Cr. | Mo. | Ni. | Vi |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HII | ≤0.20 | 0.80-1.40 | 0.015 | ≤0.012 | ≤0.30 | ≤0.020 | 0.03 | ≤0.40 | 0.025 | ≤ 0.020 | ≤0.30 | ≤0.08 | ≤0.30 | ≤0.02 |

HII material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and mechanical properties. It's yield strength is between 185 to 265 MPa.HII tensile strength is from 90 MPa to 530 MPa. (different min strength point at the different thickness.) More detailed information about DIN 17155 HII steel Mechanical Properties , please refer to the following table:

| Grade | Type | Thickness mm | Yield strength Mpa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KVJ) (min) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -20° | 0° | +20 |
| HII | Normalized | ≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250 | 265 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 255 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 245 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 215 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 200 | 400-530 | 22 | 27 | 34 | 40 |
|  |  |  | 185 | 390-530 | 22 | 27 | 34 | 40 |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.