DIN17100 St37-2 carbon and low alloy steel

Key words : 
St37-2 steel plate, under DIN17100 standard St37-2 steel plate, under DIN17100 standard, we can regard St37-2 steel plate as Carbon steel
St37-2 steel plate is one mainly of Carbon steel, St37-2 is a type of steel sheet under DIN17100 standard which is used to build ship, bridge, belongs to high strength sheet. St37-2 is equivalent to EN:ST37-2,JIS:SS400,ASTM:A283C and UNI:FE360B 
Equivalent grade : 
ST37-2 steel plate/sheet is in DIN17100 standard. The equal material of ST37-2 is: EN10025:1990 FE 360 c, EN 10025-2 S235JR, NFA 35-501 E24-3, BS1449 40C - JIS3106  SM400B,UNI7070 FE 360C .

| ST37-2 DIN17100 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE E 360 C |
|  | EN 10025-2 | S235JR |
|  | NFA 35-501 | E24-3 |
|  | BS1449 | 40C |
|  | JIS3106 | SM400B |
|  | UNI7070 | FE 360 C |

DIN17100 ST37-2 steel Chemical Composition % :
 
Main chemical composition in DIN17100 ST37-2 steel : Manganese max 1.4, Phosphorus max 0.045,Sulphur max 0.045. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.17 | 0.17 | -- | 1.40 | 0.045 | 0.045 |

EN10025 ST37-2 steel Mechanical Properties

DIN17100 ST37-2 steel plate/sheet for carbon steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about DIN17100 ST37-2 steel Mechanical Properties , please refer to the following table:

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t ≤ 16mm t > 16mm | 235 225 |  |  | Degree: 0 AV: 27J |
| t < 3mm t ≥ 3mm |  | 360-510 340-470 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 16 17 18 19 24 |  |

ICE steel is the professional Chinese steel exporter. We can offer you ST37-2 sheet, ST37-2 Cross Reference, ST37-2 Schematic, ST37-2 Distributor, ST37-2 Equivalent, ST37-2 Application Note, ST37-2 Data Sheet, ST37-2 component, ST37-2 Fiche Technique, ST37-2 Circuit, ST37-2 steel sheet, ST37-2 steel price. ST37-2 steel supplier, ST37-2 steel manufacturer.