DIN17100 St52-3 low alloy steel

Key words : 
St52-3 steel plate, under DIN17100 standard St52-3 steel plate, under DIN17100 standard, we can regard St52-3 steel plate as low alloy steel
St52-3 steel plate is one mainly of low alloy steel, St52-3 steel plate is alloy steel under the  DIN17100  standard which is equal to DIN17100:St52-3,JIS:SS490/SM490A,BS:50B and UNI7070:Fe510B 
Equivalent grade : 
St52-3 steel plate/sheet is in DIN17100 standard.The equal material of St52-3 is: DIN17100:1990 FE 510 B, EN 10025-2 S355JR,ASTM A572GR50, JIS SS490/SM490A,NFA 35-501 E36-2, BS1449 50B,UNI7070 FE 510 B.

| ST52-3 DIN17100 | Comparison of steel grades |
| --- | --- |
|  | DIN17100:1990 | FE 510 B |
|  | EN 10025-2 | S355JR |
|  | ASTM | A572GR50 |
|  | JIS | SS490/SM490A |
|  | NFA 35-501 | E36-2 |
|  | BS1449 | 50B |
|  | UNI7070 | FE 510 B |

DIN17100 St52-3 steel Chemical Composition % : 
 
Main chemical composition in DIN17100 St52-3 steel : Silicium max 0.55 Manganese max 1.6, Phosphorus max 0.045,Sulphur max 0.045. More detailed information, please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.24 | 0.24 | 0.55 | 1.60 | 0.045 | 0.045 |

DIN17100 St52-3 steel Mechanical Properties

DIN17100 St52-3 steel plate/sheet for low alloy steels, This kind of steel has very wide use. Because of the low Carbon content and without alloy element, carbon structural steel has the proper tensile strength, good toughness, plasticity,processing property. More detailed information about DIN17100 St52-3 steel Mechanical Properties , please refer to the following table:

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |

ICE steel is the professional Chinese steel exporter. We can offer you St52-3 sheet, St52-3 Cross Reference, St52-3 Schematic, St52-3 Distributor, St52-3 Equivalent, St52-3 Application Note, St52-3 Data Sheet, St52-3 component, St52-3 Fiche Technique, St52-3 Circuit, St52-3 steel sheet, St52-3 steel price. St52-3 steel supplier, St52-3 steel manufacturer.