EN 10025 E 295 steel plate/sheet for General Construction Steels

Key words :
EN10025 E295 steel plate/sheet,EN10025 E295 steel plate/sheet, under EN standard, we can regard E295 steel plate/sheet for general Construction steels.EN10025 E295 steel plate/sheet is for general Construction steels.The followings are the chemical composition and the mechanical properties of EN E295 steel.
Equivalent grade : 
E295 steel plate/sheet is in EN10025 standard. The comparison of steel grades is: EN10025 :1990 E295，DIN17100 ST50-2, NFA 35-501 A50-2,BS1449,UNI7070 FE 490.

| E295 EN 10025-2 Number: 1.0050 | Comparison of steel grades |
| --- | --- |
|  | EN10025:1990 | FE 490-2 |
|  | DIN17100 | ST50-2 |
|  | NFA 35-501 | A50-2 |
|  | BS1449 | - |
|  | UNI7070 | FE 490 |

E295 steel Chemical analysis -% by mass*
Main chemical composition in EN10025 E295 steel : Phosphorus max 0.045, Silicon max 0.045,please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. | N max |
| --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | - | - | - | - | 0.045 | 0.045 | 0.012 |

ST E295 steel Mechanical properties
EN10025 E295 is general Construction steels, The different thickness with different yield strength, tensile strength and fracture elongation. More detailed information about EN10025 E295 steel Mechanical Properties , please refer to the following table:

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 295 285 |  |  | - - |
| t < 3mm t ≥ 3mm |  | 490-600 470-610 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 11 12 13 14 18 |  |

ICE steel is the professional Chinese steel exporter. We will use our professional services , best quality and competitive price to fullfill each customers needs in steel plate.