EN 10025 FE 490-2 steel plate/sheet for general Construction steels
Key words :
EN 10025 FE 490-2 steel plate/sheet, EN 10025  FE 490-2 steel plate/sheet, under EN standard, we can regard FE 490-2 steel plate/sheet for general Construction steels. EN 10025 FE 490-2 steel plate/sheet is for general Construction steels. The followings are the chemical composition and the mechanical properties of EN FE 490-2 steel.
Equivalent grade : 
E295 steel plate/sheet is in EN10025 standard. The comparison of steel grades is: EN10025 :1990 FE 490-2，DIN17100 ST50-2, NFA 35-501 A50-2,BS1449,UNI7070 FE 490.

| FE 490-2 EN 10025-2 Number: 1.0050 | Comparison of steel grades |
| --- | --- |
|  | EN 10025 :1990 | FE 490-2 |
|  | DIN17100 | ST50-2 |
|  | NFA 35-501 | A50-2 |
|  | BS1449 | - |
|  | UNI7070 | FE 490 |

FE 490-2 steel Chemical analysis
Main chemical composition in EN 10025 FE 490-2 steel : Phosphorus max 0.045, Silicon max 0.045,please refer to the flowing table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. | N max |
| --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | - | - | - | - | 0.045 | 0.045 | 0.012 |

ST FE 490-2 steel Mechanical properties 
EN 10025 FE 490-2 is general Construction steels, The different thickness with different yield strength, tensile strength and fracture elongation. More detailed information about EN 10025 FE 490-2 steel Mechanical Properties , please refer to the following table:

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 295 285 |  |  | - - |
| t < 3mm t ≥ 3mm |  | 490-600 470-610 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 11 12 13 14 18 |  |

ICE steel is the professional Chinese steel exporter. We will use our professional services , best quality and competitive price to fullfill each customers needs in steel plate.