EN 10025 S275JR steel plate/sheetfor general purpose structural steels

Key words: S275JR steel plate/sheet, EN 10025 S275JR steel plate/sheet, S275JR steel plate/sheet supplier/Chinese supplier, S275JR steel plate/sheet price, S275JR steel plate/sheet mechanical property.

EN 10025 S275JR steel equivalent grade:
S275JR steel plate/sheet is in EN 10025 standard, the material number is 1.0044. The equivalent grades of S275JR steel are DIN 17100 St 44-2, NFA 35-501 E 28-2, UNI 7070 Fe 430 B, BS 4360 43 B, UNE 36.080 AE 275 B, ASTM A 283 D - A 36, JIS G3101 SS 400.

| S275JR EN 10025 Material #:1.0044 | Comparision of steel grades |
| --- | --- |
|  | DIN 17100 | St 44-2 |
|  | NFA 35-501 | E 28-2 |
|  | UNI 7070 | Fe 430 B |
|  | BS 4360 | 43 B |
|  | UNE 36.080 | AE 275 B |
|  | ASTM | A 283 D - A 36 |
|  | JIS G3101 | SS 400 |

EN 10025 S275JR steel chemical composition %:
Main chemical composition in EN 10025 S235JR steel is carton max 0.21, manganese max 1.50, phosphorus max 0.045, Sulphur max 0.045. More detailed information about S275JR steel, please refer to the down table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.21 | 0.21 | -- | 1.50 | 0.045 | 0.045 |

EN 10025 S275JR steel mechanical property:
S275JR steel plate, under EN10025 standard, we can regard S275JR steel plate as Carbon and low alloy steel.

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 275 265 |  |  | 20 degree 27J |
| t < 3mm t ≥ 3mm |  | 430-580 410-560 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10025 S275JR steel are available, so if need, welcome to contact ICE steel sales team.