EN 10025 S355J0 steel plate/sheet for general purpose structural steels

Key words: S355J0 steel plate/sheet, EN 10025 S355J0 steel plate/sheet, S355J0 steel plate/sheet supplier/Chinese supplier, S355J0 steel plate/sheet price, S355J0 steel plate/sheet mechanical property.

EN 10025 S355J0 steel equivalent grade:
S355J0 steel plate/sheet is in EN 10025 standard, the material number is 1.0553. The equivalent grades of S355J0 steel are DIN 17100 St 52-3 U, NFA 35-501 E 36-3, UNI 7070 Fe 510 C, BS 4360 50 C, ASTM A 441, UNE 36.080 AE 355 C.

| S355J0 EN 10025 Material #:1.0553 | Comparision of steel grades |
| --- | --- |
|  | NFA 35-501 | E 36-3 |
|  | UNI 7070 | Fe 510 C |
|  | BS 4360 | 50 C |
|  | ASTM | A 441 |
|  | UNE 36.080 | AE 355 C |
|  | DIN 17100 | St 52-3 U |

EN 10025 355J0 steel chemical composition %:
Main chemical composition in EN 10025 S355J0 steel is carton max 0.20, silicon max 0.55, manganese max 1.60, phosphorus max 0.045, Sulphur max 0.040. More detailed information about S355J0 steel, please refer to the down table:

| Chemical elements | C≤ 16mm max | C>16mm max | Si max | Mn max | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.20 | 0.55 | 1.60 | 0.040 | 0.040 |

EN 10025 355J0 steel mechanical property:
S355J0 steel plate is one mainly of carbon and low alloy steel, S355J0 steel plate is a type of steel sheet under EN standard which is used to build ship, bridge, belongs to high strength sheet.

| thickness | Yield Strength ReH [N/mm2] transv.min. | Tensile Strength Rm [N/mm2] transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | 0 degree 27J |
| t < 3mm t ≥ 3mm |  | 510-680 490-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 13 14 15 16 20 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10025 S355J0 steel are available, so if need, welcome to contact ICE steel sales team.