EN 10025 S355K2G3 steel plate/sheet for general purpose structural steels

Key words: S355K2G3 steel plate/sheet, EN 10025 S355K2G3 steel plate/sheet, S355K2G3 steel plate/sheet supplier/Chinese supplier, S355K2G3 steel plate/sheet price, S355K2G3 steel plate/sheet mechanical property.

EN 10025 S355K2G3 steel equivalent grade:
S355K2G3 steel plate/sheet is in EN 10025 standard, the material number is 1.0595. The equivalent grades of S355K2G3 steel are NFA 35-501 E 36-4, BS 4360 50 DD.

| S355K2G3 EN 10025 Material #:1.0595 | Comparison of steel grades |
| --- | --- |
|  | NFA 35-501 | E 36-4 |
|  | BS 4360 | 50 DD |

EN 10025 355K2G3 steel chemical composition %:
Main chemical composition in EN 10025 S355K2G3 steel is carton max 0.2, silicon max 0.55, manganese max 1.60, phosphorus max 0.035, sulphur max 0.035. More detailed information about S355K2G3 steel, please refer to the down table:

| Chemical elements | C≤ 16mm | C>16mmmax | Si max | Mnmax | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.2 | 0.2 | 0.55 | 1.6 | 0.035 | 0.035 |

EN 10025 355K2G3 steel mechanical property:
S355K2G3 steel plate has a -20 degree temperature steel. Compare with S355J2 , S355K2 steel plate impact energy is 40J, S355J2 is 27J under 150mm thickness. So S355K2 steel plate is better for choice in low temperature high impact energy projects.

| thickness | Yield StrengthReH[N/mm2] transv.min. | T[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm | 355 |  |  | -20 degree |
|  | 345 |  |  |  |
| t < 3mm |  | 510-680 |  |  |
| t ≥ 3mm |  | 490-630 |  |  |
| Up to 1.5mm |  |  | 13 | 40J |
| 1.51-2.00mm |  |  | 14 |  |
| 2.01-2.50mm |  |  | 15 |  |
| 2.51-2.99mm |  |  | 16 |  |
| ≥ 3mm |  |  | 20 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10025 S355K2G3 steel are available, so if need, welcome to contact ICE steel sales team.