EN 10025 S355K2G4 steel plate/sheet for general purpose structural steels

Key words: S355K2G4 steel plate/sheet, EN 10025 S355K2G4 steel plate/sheet, S355K2G4 steel plate/sheet supplier/Chinese supplier, S355K2G4 steel plate/sheet price, S355K2G4 steel plate/sheet mechanical property.

EN 10025 355K2G4 steel chemical composition %:
Main chemical composition in EN 10025 S355K2G4 steel is carton max 0.2, silicon max 0.55, manganese max 1.60, phosphorus max 0.035, sulphur max 0.035. More detailed information about S355K2G4 steel, please refer to the down table:

| Chemical elements | C≤ 16mmmax | C>16mmmax | Si max | Mnmax | P max. | S max. |
| --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.2 | 0.2 | 0.55 | 1.6 | 0.035 | 0.035 |

EN 10025 355K2G4 steel mechanical property:
S355 K2G4 steel plate is one mainly of carbon and low alloy steel, S355K2G4 steel plate is a type of steel sheet under EN standard which is used to build ship, bridge, belongs to high strength sheet.

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mmt >16mm | 355 |  |  | -20 degree |
|  | 345 |  |  |  |
| t < 3mm |  | 510-680 |  |  |
| t ≥ 3mm |  | 490-630 |  |  |
| Up to 1.5mm |  |  | 13 | 40J |
| 1.51-2.00mm |  |  | 14 |  |
| 2.01-2.50mm |  |  | 15 |  |
| 2.51-2.99mm |  |  | 16 |  |
| ≥ 3mm |  |  | 20 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10025 S355K2G4 steel are available, so if need, welcome to contact ICE steel sales team.