EN10028 P235GH steel plate/sheet for Boiler and Pressure Vessel

P235GH steel plate/sheet, P235GH steel plate/sheet metal, EN10028 P235GH steel plate/sheet for boiler steel, P235GH carbon steel used for boiler, EN10028 steel plate for boiler using, P235GH steel supplier/Chinese supplier, P235GH steel price,P235GH steel manufacturer.

P235GH steel plate/sheet is in EN10028-2 standard. It's grade Number is 1.0345. The equal material of P235GH is: DIN 17155 HI, NFA 36-205 A 37 CP, UNI 5869 Fe 360 - 1KW, BS 1501 161 Gr. 360 / 164 Gr. 360, UNE 36087 A 37 RCI, ASTM A 285 Gr. C-A 414 Gr. C / A 516 Gr. 55,JIS G3115 SPV 24.

| P235GH EN 10028-2 Number:1.0345 | DIN 17155 | HI |
| --- | --- | --- |
|  | NFA 36-205 | A 37 CP |
|  | UNI 5869 | Fe 360 - 1KW |
|  | BS 1501 | 161 Gr. 360 / 164 Gr. 360 |
|  | UNE 36087 | A 37 RCI |
|  | ASTM | A 285 Gr. C-A 414 Gr. C / A 516 Gr. 55 |
|  | JIS G3115 | SPV 24 |

Main chemical composition in EN10028-2 P235GH steel : Carbon:max 0.16 , Manganese from 0.60 to 1.20, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.35, More detailed information, please refer to the flowing table:

| Grades | C max | Si max | Mn. max | P max | S max | N max | AL min | Cr max | Cu max | Mo max | Ni max | Nb max | Ti max | V max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P235GH | 0.16 | 0.35 | 0.60-1.20 | 0.025 | 0.015 | 0.012 | 0.02 | 0.3 | 0.03 | 0.08 | 0.3 | 0.02 | 0.03 | 0.02 |

P235GH this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 170-235 MPa (there is different min strength point at the different thickness.) P235GH tensile strength is from 350 MPa to 480 MPa. (different min strength point at the different thickness.) More detailed information about EN10028-2 P235GH steel Mechanical Properties , please refer to the following table:

| Grade | Thickness (mm) | Yield Strength MPa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KV J) (min) |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | -20℃ | 0℃ | 20℃ |
| P235GH | ≤ 16 | 235 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 16＜t ≤40 | 225 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 40＜t ≤60 | 215 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 6＜t ≤100 | 200 | 360 to 480 | 24 | 27 | 34 | 40 |
|  | 100＜t ≤150 | 185 | 350 to 480 | 24 | 27 | 34 | 40 |
|  | 150＜t ≤250 | 170 | 350 to 480 | 24 | 27 | 34 | 40 |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.