EN10028 P265GH steel plate/sheet for Boiler and Pressure Vessel

P265GH steel plate/sheet, P265GH steel plate/sheet metal, EN10028 P265GH steel plate/sheet for boiler steel, P265GH carbon steel used for boiler, EN10028 steel plate for boiler using, P265GH steel supplier/Chinese supplier, P265GH steel price,P265GH steel manufacturer.

P265GH steel plate/sheet is in EN10028-2 standard. It's grade Number is 1.0481. The equal material of P265GH is: DIN 17155 HII, NFA 36-205 A 42 CP, UNI 5869 Fe 410 - 1KW, BS 1501 161 Gr. 400 / 164 Gr. 400, UNE 36087 A 42 RCI, ASTM A 414 Gr. E / A 516 Gr. 60.

| P265GH EN 10028-2 Number:1.0481 | DIN 17155 | HII |
| --- | --- | --- |
|  | NFA 36-205 | A 42 CP |
|  | UNI 5869 | Fe 410 - 1KW |
|  | BS 1501 | 161 Gr. 400 / 164 Gr. 400 |
|  | UNE 36087 | A42 RCI |
|  | ASTM | A 414 Gr. E / A 516 Gr. 60 |
|  | JIS G3115 | - |

Main chemical composition in EN10028-2 P265GH steel : Carbon:max 0.20 , Manganese from 0.80 to 1.40, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.40, More detailed information, please refer to the flowing table:

| Grade | C. % | Mn.% | S. | N | Cu | Nb | Ti. | Si. | P. | AL | Cr. | Mo. | Ni | Vi |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P265GH | 0.20 | 0.80-1.40 | 0.015 | 0.012 | 0.30 | 0.020 | 0.03 | 0.40 | 0.025 | 0.020 | 0.30 | 0.08 | 0.30 | 0.02 |

P265GH this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 185-265 MPa (there is different min strength point at the different thickness.) P265GH tensile strength is from 390 MPa to 530 MPa. (different min strength point at the different thickness.) More detailed information about EN10028-2 P265GH steel Mechanical Properties , please refer to the following table:

| Grade | Type | Thickness mm | Yield strength Mpa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KVJ) (min) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -20° | 0° | +20 |
| P265GH | Normalized | ≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250 | 265 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 255 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 245 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 215 | 410-530 | 22 | 27 | 34 | 40 |
|  |  |  | 200 | 400-530 | 22 | 27 | 34 | 40 |
|  |  |  | 185 | 390-530 | 22 | 27 | 34 | 40 |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.