EN10028 P355GH steel plate/sheet for Boiler and Pressure Vessel

P355GH steel plate/sheet, P355GH steel plate/sheet metal, EN10028 P355GH steel plate/sheet for boiler steel, P355GH carbon steel used for boiler, EN10028 steel plate for boiler using, P355GH steel supplier/Chinese supplier, P355GH steel price,P355GH steel manufacturer.

| P355GH EN 10028-2 Number:1.0473 | DIN 17155 | 19 Mn 6 |
| --- | --- | --- |
|  | NFA 36-205 | A 52 CP |
|  | UNI 5869 | Fe 510 - 1KW |
|  | BS 1501 | - |
|  | UNE 36087 | A52 RCI |
|  | ASTM | A 414 Gr. G |
|  | JIS G3115 | SPV 36 |

P355GH steel plate/sheet is in EN10028-2 standard. It's grade Number is 1.0473. The equal material of P355GH is: DIN 17155 19 Mn 6, NFA 36-205 A 52 CP, UNI 5869 Fe 510 - 1KW, UNE 36087 A 52 RCI, ASTM A 414 Gr. G,JIS G3115 SPV 36.

Main chemical composition in EN10028-2 P355GH steel : Carbon:from 0.10 to 0.22, Manganese from 0.10 to 1.70, Sulphur max 0.015, Phosphorus max 0.025, Silicon max 0.60, More detailed information, please refer to the flowing table:

| Grade | C. % | Mn.% | S. | N | Cu | Nb | Ti. | Si. | P. | AL | Cr. | Mo. | Ni | Vi |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P355GH | 0.10-0.22 | 0.10-1.70 | 0.015 | 0.012 | 0.30 | 0.020 | 0.03 | 0.60 | 0.025 | 0.020 | 0.30 | 0.08 | 0.30 | 0.02 |

P355GH this material is mainly used to fabricate boiler and pressure vessel. So ,same the other boiler and pressure vessel using steel plate, this kind of steel has the good grain and Mechanical properties. It's yield strength is between 280-355 MPa (there is different min strength point at the different thickness.) P355GH tensile strength is from 470 MPa to 650 MPa. (different min strength point at the different thickness.) More detailed information about EN10028-2 P355GH steel Mechanical Properties , please refer to the following table:

| Grade | Type | Thickness mm | Yield strength Mpa(min) | Tensile Strength MPa | Elongation % (min) | Impact Energy (KVJ) (min) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | -20° | 0° | +20 |
| P355GH | Normalized | ≤16 16>to≤40 40>to≤60 60>to≤100 100>to≤150 150>to≤250 | 355 | 510-650 | 20 | 27 | 34 | 40 |
|  |  |  | 345 | 510-650 | 20 | 27 | 34 | 40 |
|  |  |  | 335 | 460-580 | 20 | 27 | 34 | 40 |
|  |  |  | 315 | 490-630 | 20 | 27 | 34 | 40 |
|  |  |  | 295 | 480-630 | 20 | 27 | 34 | 40 |
|  |  |  | 280 | 470-630 | 20 | 27 | 34 | 40 |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.