EN 10083 C35 steel plate high carbon steel 
C35 steel plate, EN 10083 C35 steel plate, C35 high carbon steel plate and sheet, EN10083 steel plate, C35 carbon steel supplier/Chinese C35 steel supplier, C35 steel price,C35 steel manufacturer.

C35 steel plate is one mainly of high carbon steel,the application of EN 10083 C35 steel plate is equal to JIS G4051 S35C,DIN C35,UNI C35,NFA AF55-C35 ,UNE36011 C35K and AISI 1035.

| C35 EN 10083-2 Number:1.0501 | Comparison of steel grades |
| --- | --- |
|  | JIS G 4051 | S 35 C |
|  | DIN 17200 | C 35 |
|  | NFA 33-101 | AF55-C 35 |
|  | UNI 7846 | C 35 |
|  | BS 970 | 070 M 36 |
|  | UNE 36011 | C 35 k |
|  | SAE J 403-AISI | 1035 |

Main chemical composition in EN10083-2 C35 steel : Carbon: from 0.32 to 0.39 , Manganese from 0.50 to 0.80, Sulphur max 0.025, Phosphorus max 0.025, Silicon from 0.15 to 0.35, More detailed information, please refer to the flowing table:
C35 steel Chemical Composition

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| C35 | 0.32-0.39 | 0.15-0.35 | 0.50-0.80 | 0.025 | 0.025 | 0.20-0.40 |

C35 high carbon steel has the good grain and Mechanical properties. It's yield strength is between 310-440 MPa ,C35 tensile strength is from 480MPa to 1690MPa. More detailed information about EN10083-2 C35 steel Mechanical Properties , please refer to the following table:

C35 steel Mechanical Properties

| Grade | Condition | Yield Strength R° (Mpa) | Tensile Strength Rm (Mpa) | Elongation A5(%) | Hardness HRC | Quenching Temperature (℃) | Bend ability | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| C35 | Rolled Annealed Water-quenched Oil quenched | 440 310 | 700 480 1845 1690 | 18 30 | 53 50 | 840 880 | Min.recommended Bending radius (≤90°) | 2.0 ×t | 1.0×t |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like EN 10083-2 C35 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  EN 10083-2 C35 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.