EN 10083 C40 steel plate high carbon steel 
C40 steel plate, EN 10083 C40 steel plate, C40 high carbon steel plate and sheet, EN10083 steel plate, C40 carbon steel supplier/Chinese C40 steel supplier, C40 steel price,C40 steel manufacturer.

C40 steel plate is one mainly of high carbon steel,the application of EN 10083 C40 steel plate is equal to JUS Č.14341,DIN C40,UNI C40,NFA AF60-C40 ,and AISI 1040.

| C40 EN 10083-2 Number: 1.0511 | Comparison of steel grades |
| --- | --- |
|  | JUS | Č.14341 |
|  | DIN | C40 |
|  | BS | 080M40, EN8 |
|  | GOST | 40 |
|  | AISI | 1040 |
|  | UNI | C40, |
|  | NF | (AF60C40), (1C40) |

Main chemical composition in EN10083-2 C40 steel : Carbon: from 0.37 to 0.44 , Manganese from 0.50 to 0.80, Sulphur max 0.045, Phosphorus max 0.045, Silicon max 0.40, More detailed information, please refer to the flowing table:
Chemical Composition of C40 steel

| Chemical elements | C | Si max. | Mn | P max. | S max. | Cr max. | Mo max. | Ni max. | Cr+Mo+Ni max. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %, by mass | 0,37-0,44 | 0,40 | 0,50-0,80 | 0,045 | 0,045 | 0,40 | 0,10 | 0,40 | 0,63 |
| Permissible deviation | ± 0,02 | + 0,03 | ± 0,04 | + 0,005 | + 0,005 | + 0,05 | + 0,03 | + 0,05 |  |

C40 high carbon steel has the good grain and Mechanical properties. It's yield strength is between 290-550 MPa ,C40 tensile strength is from 260MPa to 530MPa. More detailed information about EN10083-2 C40 steel Mechanical Properties , please refer to the following table:

C40 steel Mechanical Properties

| Thickness of ruling section tR |
| --- |
| Diameter in mm | tR ≤ 100mm | 100< tR ≤250mm | 250< tR ≤500mm | 500< tR ≤1000mm |
| Re min (N/mm2) | 290 | 260 | - | - |
| Rm min (N/mm2) | 550 | 530 | - | - |
| A % min. | l-longitudinal | 17 | 17 | - | - |
|  | tr -transverse | - | - | - | - |
| KV min * (J) | l-longitudinal | - | - | - | - |
|  | tr -transverse | - | - | - | - |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like EN 10083-2 C40 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  EN 10083-2 C40 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.