EN 10083 C45 steel plate high carbon steel 
C45 steel plate, EN 10083 C45 steel plate, C45 high carbon steel plate and sheet, EN10083 steel plate, C45 carbon steel supplier/Chinese C45 steel supplier, C45 steel price,C45 steel manufacturer.

C45 steel plate is one mainly of high carbon steel,the application of EN 10083 C45 steel plate is equal to JIS G4051 S45C,DIN17200 C45,UNI7846 C45,NFA AF65-C45 ,UNE36011 C45K and AISI 1042/1045.

| C45 EN 10083-2 Number:1.0503 | Comparison of steel grades |
| --- | --- |
|  | JIS G 4051 | S 45 C |
|  | DIN 17200 | C 45 |
|  | NFA 33-101 | AF65-C 45 |
|  | UNI 7846 | C 45 |
|  | BS 970 | 070 M 46 |
|  | UNE 36011 | C 45 k |
|  | SAE J 403-AISI | 1042/1045 |

Main chemical composition in EN10083-2 C45 steel : Carbon: from 0.42 to 0.50, Manganese from 0.50 to 0.80, Sulphur max 0.025, Phosphorus max 0.025, Silicon from 0.15 to 0.35, More detailed information, please refer to the flowing table:
Chemical Composition of C45 steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| C45 | 0.42-0.50 | 0.15-0.35 | 0.50-0.80 | 0.025 | 0.025 | 0.20-0.40 |

C45 high carbon steel has the good grain and Mechanical properties. It's yield strength is between 330-460 MPa ,C45 tensile strength is from 540MPa to 2270MPa. More detailed information about EN10083-2 C45 steel Mechanical Properties , please refer to the following table:

Mechanical Properties of C45 steel

| Grade | Condition | Yield Strength R°(Mpa) | Tensile Strength Rm (Mpa) | Elongation A5(%) | Hardness HRC | Quenching Temperature (℃) | Bend ability | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| C45 | Rolled Annealed Water-quenched Oil quenched | 460 330 | 750 540 2270 1980 | 18 30 | 58 55 | 820 860 | Min.recommended Bending radius (≤90°) | 2.0 ×t | 1.0×t |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like EN 10083-2 C45 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  EN 10083-2 C45 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.