EN 10083 C50 steel plate high carbon steel 
C50 steel plate, EN 10083 C50 steel plate, C50 high carbon steel plate and sheet, EN10083 steel plate, C50 carbon steel supplier/Chinese C50 steel supplier, C50 steel price,C50 steel manufacturer.

C50 steel plate is one mainly of high carbon steel,the application of EN 10083 C50 steel plate is equal to JUS Č.16301,DIN17200 C50,NF AF70C55,JIS G 4051 S 50 C，SAE J 403-AISI 1049 / 1050,BS970 070 M 50.

| C50 EN 10083-2 Number: 1.0540 | Comparison of steel grades |
| --- | --- |
|  | JUS | Č.16301 |
|  | DIN | C50 |
|  | BS970 | 070 M 50 |
|  | GOST | - |
|  | SAE J 403-AISI | 1049 / 1050 |
|  | JIS G 4051 | S 50 C |
|  | NF | (AF70C55) |

Main chemical composition in EN10083-2 C50 steel : Carbon: from 0.47 to 0.55, Manganese from 0.60 to 0.90, Sulphur max 0.045, Phosphorus max 0.045, Silicon max 0.40, More detailed information, please refer to the flowing table:
Chemical Composition of C50 steel

| Chemical elements | C | Si max. | Mn | P max. | S max. | Cr max. | Mo max. | Ni max. | Cr+Mo+Ni max. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %, by mass | 0,47-0,55 | 0,40 | 0,60-0,90 | 0,045 | 0,045 | 0,40 | 0,10 | 0,40 | 0,63 - - |
| Permissible deviation | ± 0,02 | + 0,03 | ± 0,04 | + 0,005 | + 0,005 | + 0,05 | + 0,03 | + 0,05 |  |

C50 high carbon steel has the good grain and Mechanical properties. It's yield strength is between 320-610 MPa ,C50 tensile strength is from290MPa to 590MPa. More detailed information about EN10083-2 C50 steel Mechanical Properties , please refer to the following table:

Mechanical Properties of C50 steel

| Thickness of ruling section tR |
| --- |
| Diameter in mm | tR ≤ 100mm | 100< tR≤250mm | 250< tR≤500mm | 500< tR≤1000mm |
| Re min (N/mm2) | 320 | 290 | - | - |
| Rm min (N/mm2) | 610 | 590 | - | - |
| A % min. | l-longitudinal | 14 | 14 | - | - |
|  | tr -transverse | - | - | - | - |
| KV min * (J) | l-longitudinal | - | - | - | - |
|  | tr -transverse | - | - | - | - |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like EN 10083-2 C50 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  EN 10083-2 C50 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.