EN 10083 C55 steel plate high carbon steel 
C55 steel plate, EN 10083 C55 steel plate, C55 high carbon steel plate and sheet, EN10083 steel plate, C55 carbon steel supplier/Chinese C55 steel supplier, C55 steel price,C55 steel manufacturer.

C55 steel plate is one mainly of high carbon steel,the application of EN 10083 C55 steel plate is equal to DIN17200 C55,NF AF70C55,JIS G 4051 S 55 C，SAE J 403-AISI 1055,BS970 070 M 55.

| C55 EN 10083-2 Number:1.0535 | Comparison of steel grades |
| --- | --- |
|  | JIS G 4051 | S 55 C |
|  | DIN 17200 | C 55 |
|  | NFA 33-101 | AF70-C 55 |
|  | UNI 7846 | C 55 |
|  | BS 970 | 070 M 55 |
|  | UNE 36011 | C 55 k |
|  | SAE J 403-AISI | 1055 |

Main chemical composition in EN10083-2 C55 steel : Carbon: from 0.52 to 0.60, Manganese from 0.60 to 0.90, Sulphur max 0.025, Phosphorus max 0.025, Silicon from 0.15 to 0.35, More detailed information, please refer to the flowing table:
Chemical Composition of C55 steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| C55 | 0.52-0.60 | 0.15-0.35 | 0.60-0.90 | 0.025 | 0.025 | 0.20-0.40 |

C55 high carbon steel has the good grain and Mechanical properties. It's yield strength is between 350-500 MPa ,C55 tensile strength is from550MPa to 2510MPa. More detailed information about EN10083-2 C55 steel Mechanical Properties , please refer to the following table:

Mechanical Properties of C55 steel

| Grade | Condition | Yield Strength R°(Mpa) | Tensile Strength Rm (Mpa) | Elongation A5(%) | Hardness HRC | Quenching Temperature (℃) | Bend ability | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| C55 | Rolled Annealed Water-quenched Oil quenched | 500 350 | 825 550 2510 2120 | 18 30 | 61 57 | 805 845 | Min.recommended Bending radius (≤90°) | 3.0 ×t | 1.0×t |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like EN 10083-2 C55 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  EN 10083-2 C55 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services.