EN 10083 C60 steel plate high carbon steel 
C60 steel plate, EN 10083 C60 steel plate, C60 high carbon steel plate and sheet, EN10083 steel plate, C60 carbon steel supplier/Chinese C60 steel supplier, C60 steel price,C60 steel manufacturer.

C60 steel plate is one mainly of high carbon steel,the application of EN 10083 C60 steel plate is equal to DIN17200 C60,JIS G 4051 S 58 C，SAE J 403-AISI 1060,BS970 070 M 60.

| C60 EN 10083-2 Number:1.0601 | Comparison of steel grades |
| --- | --- |
|  | JIS G 4051 | S 58 C |
|  | DIN 17200 | C 60 |
|  | NFA 33-101 | - |
|  | UNI 7846 | - |
|  | BS 970 | 070 M 60 |
|  | UNE 36011 | - |
|  | SAE J 403-AISI | 1060 |

Main chemical composition in EN10083-2 C60 steel : Carbon: from 0.57 to 0.65, Manganese from 0.60 to 0.90, Sulphur max 0.025, Phosphorus max 0.025, Silicon from 0.15 to 0.35, More detailed information, please refer to the flowing table:
Chemical Composition of C60 steel

| Grade | C(%)min-max | Si(%)min-max | Mn(%)min-max | P(%)max | S(%)max | Cr(%)min-max |
| --- | --- | --- | --- | --- | --- | --- |
| C60 | 0.57-0.65 | 0.15-0.35 | 0.60-0.90 | 0.025 | 0.025 | 0.20-0.40 |

C60 high carbon steel has the good grain and Mechanical properties. It's yield strength is between 350-500 MPa ,C60 tensile strength is from550MPa to 2510 MPa. More detailed information about EN10083-2 C60 steel Mechanical Properties , please refer to the following table:

Mechanical Properties of C60 steel

| Grade | Condition | Yield Strength R°(Mpa) | Tensile Strength Rm (Mpa) | Elongation A5(%) | Hardness HRC | Quenching Temperature (℃) | Bend ability | Nominal Thickness,t 1.95mm≤t≤10.0mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rolled | Annealed |
| C60 | Rolled Annealed Water-quenched Oil quenched | 500 350 | 825 550 2510 2120 | 18 30 | 61 57 | 805 845 | Min.recommended Bending radius (≤90°) | 3.0 ×t | 1.0×t |

ICE steel is the professional Chinese steel exporter,we can supply all kinds of steel products like EN 10083-2 C60 steel plate,steel sheet,metal sheet,flanges,steel circle, color coated steel plate, hot plate, steel coils, etc.If our products  EN 10083-2 C60 steels are helpful to you,please be free to contact,we promise to give you the most competitive prices and best services