EN 10111 S275NL steel plate/sheet for fine-grain structural steel
Key words: S275NL steel plate/sheet, EN 10111 S275NL steel plate/sheet, S275NL steel plate/sheet supplier/Chinese supplier, S275NL steel plate/sheet price, S275NL steel plate/sheet mechanical property.

EN 10111 S275NL steel Equivalent grade:
S275NL steel plate/sheet is in EN 10111 standard, the grade number is 1.0491. The equivalent materials of S275NL steel are UNE36081 AE 285 KT, DIN17102 T StE 285, UN Fe E 275 KT N, BS4360 43 EE.

| S275NL EN 10111 MATERIAL# 1.0491 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE 285 KT |
|  | DIN17102 | T StE 285 |
|  | UN | Fe E 275 KT N |
|  | BS4360 | 43 EE |

EN 10111 S275NL steel chemical composition %:
Main chemical composition in EN 10111 S275NL steel is carton max 0.16, silicon max 0.40, manganese from 0.50-1.50, phosphorus max 0.025, Sulphur max 0.020, chromium max 0.30.
More detailed information about S275NL steel, please refer to the down table:

| Chemical elements | C max | Si max | Mn max | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.16 | 0.40 | 0.50-1.50 | 0.025 | 0.020 | 0.55 | 0.30 | 0.30 | 0.05 | 0.05 | 0.02 |

EN 10111 S275NL steel mechanical property:
S275NL steel plate is one mainly of Fine-grain structural steels, normalised rolled steel, S275NL steel plate is a hot rolled structural steels, which technical delivery conditions for normalized or normalized rolled in weldable fine grain structural steel grade. It is also regarded as DIN:TStE285 and BS:43EE

| thickness | Yield StrengthReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 275 265 |  |  | +20 KV 40J 0 KV 34J -10 KV 30J -20 KV 27J -30 KV 23J -40 KV 20J -50 KV 16J |
| t < 3mm t ≥ 3mm |  | 370-510 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 24 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10111 S275NL steel are available, so if need, welcome to contact ICE steel sales team.