EN 10111 S355N steel plate/sheet for fine-grain structural steel
Key words: S355N steel plate/sheet, EN 10111 S355N steel plate/sheet, S355N steel plate/sheet supplier/Chinese supplier, S355N steel plate/sheet price, S355N steel plate/sheet mechanical property.

EN 10111 S355N steel Equivalent grade: 
S355N steel plate/sheet is in EN 10111 standard, the grade number is 1.0545. The equivalent materials of S355N steel are UNE36081 AE355KG/AE355KW, DIN17102 STE355, NFA 36-201 E355R, UN Fe E 3555KG N.

| S355N EN 10111 MATERIAL#1.0545 | Comparison of steel grades |
| --- | --- |
|  | UNE36081 | AE355KG/AE355KW |
|  | DIN17102 | STE355 |
|  | NFA 36-201 | E355R |
|  | UN | ccc |

EN 10111 S355N steel chemical composition %: 
Main chemical composition of EN 10111 S355N steel is carton max 0.20, silicon max 0.50, manganese from 0.90-1.65, phosphorus max 0.030, Sulphur max 0.025, chromium max 0.30. More detailed information about S355N steel, please refer to the down table:

| Chemical elements | C max | Si max | Mn | P max | S max. | Cu max | Cr max | Ni max | V max | Nb max | Al min |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| %,by mass | 0.20 | 0.50 | 0.90-1.65 | 0.030 | 0.025 | 0.55 | 0.30 | 0.50 | 0.12 | 0.05 | 0.02 |

EN 10111 S355N steel mechanical property:
S355N steel plate is one mainly of Fine-grain structural steels, normalised rolled steel, S355N steel plate under EN10111 standard, it is normalized , fine grain structural steel. More detailed information about S355N steel, please refer to the down table:

| thickness | Yield Strength ReH[N/mm2] transv.min. | TensileStrengthRm[N/mm2]transv. | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| t≤ 16mm t >16mm | 355 345 |  |  | +20 KV 31J 0 KV 27J -10 KV 24J -20 KV 20J -40 - -50 - |
| t < 3mm t ≥ 3mm |  | 470-630 |  |  |
| Up to 1.5mm 1.51-2.00mm 2.01-2.50mm 2.51-2.99mm ≥ 3mm |  |  | 22 |  |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10111 S355N steel are available, so if need, welcome to contact ICE steel sales team.