EN 10111 S420NLsteel plate/sheet for fine-grain structural steel
Key words: S420NL steel plate/sheet, EN 10111 S420NL steel plate/sheet, S420NL steel plate/sheet supplier/Chinese supplier, S420NL steel plate/sheet price, S420NL steel plate/sheet mechanical property.

EN 10111 S420NL steel equivalent grade:
S420NL steel plate/sheet is in EN 10111 standard, the grade number is 1.8912. The The equivalent materials of S420N steel are DIN 1614/2 TStE 420, NFA 36-301 NFA 36-301, BS 1449 50 F, ASTM - SAE A 633 Gr. E / A 572 Gr. 60 / A 738 Gr. C.

| S420N EN 10111 Material # 1.8902 | DIN 1614/2 | NFA 36-301 | BS 1449 | ASTM - SAE |
| --- | --- | --- | --- | --- |
|  | TStE 420 | E 420 FP | 50 F | A 633 Gr. E / A 572 Gr. 60 / A 738 Gr. C |

EN 10111 S420NL steel chemical composition %: 
Main chemical composition of EN 10111 S420NL steel is carton max 0.20, silicon max 0.60, manganese from 1.0-1.7, phosphorus max 0.025, Sulphur max 0.02, chromium max 0.30. More detailed information about S420NL steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S420NL | 0.2 | 0.6 | 1.0- 1.7 | 0.025 | 0.02 | 0.025 | 0.02 | 0.05 | 0.2 | 0.05 | 0.3 | 0.8 | 0.1 | 0.55 | 0.52 |

EN 10111 S420NL steel mechanical property:
EN 10111 S420NL steel plate/sheet is a hot rolled structural steels,which under specification EN 10025_3.The yield strength of S420NL shall be above 420Mpa for the thickness belows 16 millimeter.The tensile strength for thickness belows 100 millimeter of this steel grade S420NL shall be within 520_680Mpa.

| Grade | Yield Strength (Min Mpa) Thickness(mm) | Tensile Strength (Mpa) | Impacting Test |
| --- | --- | --- | --- |
|  | ≤ 16 | 16-40 | 40-100 | ≥ 100 | T<100 | T>100 | ℃ | J |
| S420NL | 420 | 400 | 390 | 340 | 520-680 | 500-650 | -50 | 27 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10111 S420NL steel are available, so if need, welcome to contact ICE steel sales team.