EN 10113-3 S275M steel plate/sheet for fine-grain structural steel

Key words: S275M steel plate/sheet, EN 10113-3 S275M steel plate/sheet, S275M steel plate/sheet supplier/Chinese supplier, S275M steel plate/sheet price, S275M steel plate/sheet mechanical property.

EN 10113-3 S275M steel equivalent grades:
S275M steel plate/sheet is in EN 10113-3 standard, the grade number is 1.8818. The equivalent materials of S275M steel are DIN-SEW083 StE 275 TM, UNI Fe E 275 KGTM,

| S275M EN 10113-3 Number:1.8818 | Comparision of steel grades |
| --- | --- |
|  | DIN-SEW083 | StE 275 TM |
|  | UNI | Fe E 275 KGTM |

EN 10113-3 S275M steel chemical composition %:
Main chemical composition in EN 10113-3 S275M steel is carton max 0.13, silicon max 0.50, manganese max 1.50, phosphorus max 0.025, Sulphur max 0.02, chromium max 0.30. More detailed information about S275M steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S275M | 0.13 | 0.50 | 1.5 | 0.025 | 0.02 | 0.015 | 0.02 | 0.05 | 0.08 | 0.05 | 0.30 | 0.3 | 0.10 | 0.55 | 0.38 |

EN 10113-3 S275M steel mechanical property:

EN10113 S275M is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy.

| Temperature | -10 | 0 | 20 |
| --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 43 | 47 | 55 |

| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- | --- |
| ReH-Minimun yield strength(Mpa) | 275 | 265 | 255 | 245 | 245 | 240 |

| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- |
| Rm-Tensile strength(Mpa) | 370-530 | 360-520 | 350-510 | 350-510 | 350-510 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 24 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10113-3 S275M steel are available, so if need, welcome to contact ICE steel sales team.