EN 10113-3 S275ML steel plate/sheet for fine-grain structural steel
Key words: S275ML steel plate/sheet, EN 10113-3 S275ML steel plate/sheet, S275ML steel plate/sheet supplier/Chinese supplier, S275ML steel plate/sheet price, S275ML steel plate/sheet mechanical property.

EN 10113-3 S275M steel equivalent grades:
S275ML steel plate/sheet is in EN 10113-3 standard, the grade number is 1.8819. The equivalent materials of S275ML steel are DIN-SEW083 TStE 275 TM, UNI 7382 Fe E 275 KTTM.

| S275ML EN 10113-3 Number:1.8819 | Comparision of steel grades |
| --- | --- |
|  | DIN-SEW083 | TStE 275 TM |
|  | UNI 7382 | Fe E 275 KTTM |
|  | BS 4360 | - |
|  | ASTM | - |

EN 10113-3 S275ML steel chemical composition %:
Main chemical composition in EN 10113-3 S275ML steel is carton max 0.13, silicon max 0.50, manganese max 1.50, phosphorus max 0.025, Sulphur max 0.02, chromium max 0.30. More detailed information about S275ML steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S275ML | 0.13 | 0.50 | 1.5 | 0.025 | 0.02 | 0.015 | 0.02 | 0.05 | 0.08 | 0.05 | 0.30 | 0.3 | 0.10 | 0.55 | 0.38 |

EN 10113-3 S275ML steel mechanical property:
EN10113 S275ML is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.It is according to EN10113-3 standard.S means the structural steel, M means the delivery condition. Capital letter L for the quality with specified minimum values of values of impact energy at temperature not lower than -50 degree.

| Temperature | -50 | -40 | -30 | -20 | -10 | 0 | 20 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 27 | 31 | 40 | 47 | 51 | 55 | 63 |

| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- | --- |
| ReH-Minimun yield strength(Mpa) | 275 | 265 | 255 | 245 | 245 | 240 |

| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- |
| Rm-Tensile strength(Mpa) | 370-530 | 360-520 | 350-510 | 350-510 | 350-510 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 24 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10113-3 S275ML steel are available, so if need, welcome to contact ICE steel sales team.