EN 10113-3 S355ML steel plate/sheet for fine-grain structural steel

Key words: S355ML steel plate/sheet, EN 10113-3 S355ML steel plate/sheet, S355ML steel plate/sheet supplier/Chinese supplier, S355ML steel plate/sheet price, S355ML steel plate/sheet mechanical property.

EN 10113-3 S355ML steel equivalent grades:
S355ML steel plate/sheet is in EN 10113-3 standard, the grade number is 1.8834. The equivalent materials of S355M steel are SEW 083 TStE 355 TM, NFA 36-201 E 355 FP, UNI 7382 Fe E 355 KTTM, BS 4360 50 EE, ASTM A 633 Gr.C.

| S355ML EN 10113-3 Number:1.8834 | Comparision of steel grades |
| --- | --- |
|  | SEW 083 | TStE 355 TM |
|  | NFA 36-201 | E 355 FP |
|  | UNI 7382 | Fe E 355 KTTM |
|  | BS 4360 | 50 EE |
|  | ASTM | A 633 Gr.C |

EN 10113-3 S355ML steel chemical composition %:
Main chemical composition in EN 10113-3 S355ML steel is carton max 0.14, silicon max 0.50, manganese max 1.60, phosphorus max 0.025, Sulphur max 0.025, chromium max 0.30. More detailed information about S355ML steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S355ML | 0.14% | 0.50% | 1.60% | 0.025% | 0.025% | 0.02% | 0.02% | 0.05% | 0.10% | 0.05% | 0.30% | 0.50% | 0.10% | 0.55% | 0.45% |

EN 10113-3 S355ML steel mechanical property:
EN10113-3 S355ML is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy at temperature not lower than -50 degree.

| Temperature | -50 | -40 | -30 | -20 | -10 | 0 | 20 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 27 | 31 | 40 | 47 | 51 | 55 | 63 |

| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- | --- |
| ReH-Minimun yield strength(Mpa) | 355 | 345 | 335 | 325 | 325 | 320 |

| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- |
| Rm-Tensile strength(Mpa) | 470-630 | 450-610 | 440-600 | 440-600 | 430-590 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 22 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10113-3 S355ML steel are available, so if need, welcome to contact ICE steel sales team.