EN 10113-3 S420M steel plate/sheet for fine-grain structural steel

Key words: S420M steel plate/sheet, EN 10113-3 S420M steel plate/sheet, S420M steel plate/sheet supplier/Chinese supplier, S420M steel plate/sheet price, S420M steel plate/sheet mechanical property.

EN 10113-3 S420M steel equivalent grade:
S420M steel plate/sheet is in EN 10113-3 standard, the grade number is 1.8825. The equivalent materials of S420M steel are SEW 083 TStE 420 TM, NFA 36-201 E 420 R, ASTM A 572 Gr.60.

| S420M EN 10113-3 Number:1.8825 | Comparision of steel grades |
| --- | --- |
|  | SEW 083 | TStE 420 TM |
|  | NFA 36-201 | E 420 R |
|  | UNI 7382 | - |
|  | BS 4360 | - |
|  | ASTM | A 572 Gr.60 |

EN 10113-3 S420M steel chemical composition %:
Main chemical composition in EN 10113-3 S420M steel is carton max 0.16, silicon max 0.50, manganese max 1.70, phosphorus max 0.030, Sulphur max 0.025, chromium max 0.30. More detailed information about S420M steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S420M | 0.16% | 0.50% | 1.70% | 0.03% | 0.025% | 0.025% | 0.02% | 0.05% | 0.12% | 0.05% | 0.30% | 0.80% | 0.20% | 0.55% | 0.47% |

EN 10113-3 S420M steel mechanical property:
EN10113-3 S420M is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy.

| Temperature | -10 | 0 | 20 |
| --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 43 | 47 | 55 |

| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- | --- |
| ReH-Minimun yield strength(Mpa) | 420 | 400 | 390 | 380 | 370 | 365 |

| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- |
| Rm-Tensile strength(Mpa) | 520-680 | 500-660 | 480-640 | 470-630 | 460-620 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 19 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10113-3 S420M steel are available, so if need, welcome to contact ICE steel sales team.