EN 10113-3 S460M steel plate/sheet for fine-grain structural steel

Key words: S460M steel plate/sheet, EN 10113-3 S460M steel plate/sheet, S460M steel plate/sheet supplier/Chinese supplier, S460M steel plate/sheet price, S460M steel plate/sheet mechanical property.

EN 10113-3 S460M steel equivalent grade:
S460M steel plate/sheet is in EN 10113-3 standard, the grade number is 1.8827. The equivalent materials of S460M steel are SEW 083 StE 460 TM, NFA 36-201 E 460 R, UNI 7382 Fe E 460 KGTM, ASTM A 572 Gr.65.

| S460M EN 10113-3 Number:1.8827 | Comparision of steel grades |
| --- | --- |
|  | SEW 083 | StE 460 TM |
|  | NFA 36-201 | E 460 R |
|  | UNI 7382 | Fe E 460 KGTM |
|  | BS 4360 | - |
|  | ASTM | A 572 Gr.65 |

EN 10113-3 S460M steel chemical composition %:
Main chemical composition in EN 10113-3 S460M steel is carton max 0.16, silicon max 0.60, manganese max 1.70, phosphorus max 0.030, Sulphur max 0.025, chromium max 0.30. More detailed information about S460M steel, please refer to the down table:

| Grade | C max | Si max | Mn max | P max | S max | N max | AL max | Nb max | V max | Ti max | Cr max | Ni max | Mo max | Cu max | CEV max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S460M | 0.16% | 0.60% | 1.70% | 0.03% | 0.025% | 0.025% | 0.02% | 0.05% | 0.12% | 0.05% | 0.30% | 0.80% | 0.20% | 0.55% | 0.48% |

EN 10113-3 S460M steel mechanical property:
EN10113-3 S460M is a technical delivery conditions for thermomechanical rolled weldable fine grain structural steels.S means the structural steel, M means the delivery condition.Capital letter L for the quality with specified minimum values of values of impact energy at temperature not lower than -20 degree.

| Temperature | -10 | 0 | 20 |
| --- | --- | --- | --- |
| Notch impact test. Min. absorbed energy | 43 | 47 | 55 |

| Nominal thickness(mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- | --- |
| ReH-Minimun yield strength(Mpa) | 460 | 440 | 430 | 410 | 400 | 385 |

| Nominal thickness(mm) | to 40 | 40-63 | 63-80 | 80-100 | 100-120 |
| --- | --- | --- | --- | --- | --- |
| Rm-Tensile strength(Mpa) | 540-720 | 530-710 | 510-690 | 500-680 | 490-660 |
| Nominal thickness(mm) | - |
| A-Minimum elongation Lo=5,65√So(%) | 17 |

ICE steel is the professional Chinese steel exporter, especially in fin-grain structural steel. We keep 10000 tons ex-stock in our warehouse, and the MTC and sample of EN 10113-3 S460M steel are available, so if need, welcome to contact ICE steel sales team.